Fig. 1

Fig. 2

Fig. 3

Fig. 4

Fig. 5

Fig. 6

Fig. 7

Fig. 8

Table 1 Textural and acidic properties of the sol-gel prepared B-Al2O3 supports

| B/Al* | BET Specific Surface Area (SSA; m2.g-1) | Water Pore Volume (PV; cm3.g-1) | BJH Pore Volume (PV; cm3.g-1) | Average Pore Diameter** (APD; nm) | Total Acidity*** (mmol.g-1) | Proportion of strong acid sites**** (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 363 | 1.9 | 0.84 | 9.3 | 1.58 | 85.9 |
| 0.02 | 474 | 1.95 | 0.78 | 6.4 | 2.26 | 69.5 |
| 0.04 | 532 | 1.9 | 0.82 | 6.1 | 2.51 | 64.2 |
| 0.08 | 554 | 1.75 | 0.8 | 5.6 | 1.85 | 58.2 |
| 0.20 | 485 | 1.55 | 0.59 | 4.6 | 2.07 | 65.8 |
| 0.32 | 510 | 1.55 | 0.66 | 4.9 | 2.65 | 67.7 |
| 0.49 | 616 | 1.35 | 0.87 | 5.2 | 2.42 | 56.7 |
| 0.61 | 606 | 2.6 | 1.22 | 6.8 | 4.09 | 65.2 |

* Corrected for nominal B/Al ratios larger than 0.15 (see Ref. [36] and section 2.1 in the text).

** Calculated using the BET SSA and BJH PV.

*** Total amount of adsorbed NH3 on each catalyst.

**** Ratio of strong acidity relative to the total acidity. Strong acidity was defined as the area of the high temperature peak at about 523 K.

Table 2 Physical properties of the CoMo/B-Al2O3 oxidic precursors

| Corrected B/Al* | BET Specific Surface Area (SSA) | BJH Pore Volume (PV) | Average Pore Diameter (APD**) |
| --- | --- | --- | --- |
|  | (m2.g-1) | Ratio*** (-) | (cm3.g-1) | Ratio*** (-) | (nm) | Ratio*** (-) |
| 0 | 387 | 1.1 | 0.63 | 0.71 | 6.5 | 0.70 |
| 0.02 | 368 | 0.78 | 0.59 | 0.76 | 6.4 | 1.00 |
| 0.04 | 391 | 0.47 | 0.54 | 0.41 | 5.5 | 0.90 |
| 0.08 | 358 | 0.65 | 0.46 | 0.58 | 5.1 | 0.91 |
| 0.20 | 345 | 0.71 | 0.44 | 0.75 | 5.1 | 1.11 |
| 0.32 | 365 | 0.72 | 0.49 | 0.74 | 5.4 | 1.10 |
| 0.49 | 341 | 0.56 | 0.51 | 0.60 | 6.0 | 1.15 |
| 0.61 | 342 | 0.56 | 0.77 | 0.63 | 9.0 | 1.32 |
| IRC**** | 271 | - | - | - | 7.6 | - |

* See the first footnote of Table 1.

** Calculated using the BET SSA and BJH PV.

*** Ratio relative to that of the corresponding B-Al2O3 support.

**** Industrial reference catalyst.

Table 3 Catalytic activities in HDS of thiophene

| Corrected B/Al* | HDS Rate (x 108 mol.gcat.s-1) | Product Distribution |
| --- | --- | --- |
|  |  | Cis-but-2-ene (%) | But-1-ene + Trans-but-2-ene (%) | Butane (%) |
| 0 | 120 | 40.3 | 18 | 41.7 |
| 0.02 | 186 | 29.9 | 27.6 | 42.5 |
| 0.04 | 191 | 34.7 | 31.7 | 33.6 |
| 0.08 | 176 | 31.9 | 29.6 | 38.5 |
| 0.20 | 167 | 34.7 | 31.7 | 33.6 |
| 0.32 | 137 | 39.2 | 33.5 | 27.3 |
| 0.49 | 128 | 44.8 | 34.9 | 20.3 |
| 0.61 | 108 | 41.4 | 37.5 | 21.1 |
| IRC | 135 | 39.7 | 21.8 | 38.5 |

* See the first footnote of Table 1.

Table 4 Catalytic activities in HDS reactions of DBT

| Corrected B/Al* | HDS Rate (x 106 mol.gcat-1.s-1) | Product Distribution |
| --- | --- | --- |
|  |  | Biphenyl (%) | Cyclohexylbenzene (%) | 4H-DBT** (%) | 6H-DBT***(%) |
| 0 | 4.30 | 90.6 | 7.4 | 1.8 | 0.2 |
| 0.02 | 5.79 | 92.9 | 6.1 | 1 | < 0.2 |
| 0.04 | 6.05 | 93.1 | 5.8 | 1.1 | < 0.2 |
| 0.08 | 4.22 | 94.1 | 4.5 | 1.4 | < 0.2 |
| 0.20 | 3.37 | 94.1 | 4 | 1.9 | < 0.2 |
| 0.32 | 2.94 | 92.4 | 4.8 | 2.8 | < 0.2 |
| 0.49 | 2.85 | 90.2 | 6.1 | 3.7 | < 0.2 |
| 0.61 | 1.66 | 89.7 | 6.2 | 4.1 | < 0.2 |
| IRC | 3.57 | 76.2 | 22.5 | 1.1 | 0.2 |

* See the first footnote of Table 1.

** 4H-DBT: tetrahydrodibenzothiophene.

*** 6H-DBT: hexahydrodibenzothiophene.

Table 5 Catalytic activities in HDS reactions of 4,6-DMDBT

| Corrected B/Al* | HDS Rate (x 106 mol.gcat-1.s-1) | Product Distribution |
| --- | --- | --- |
|  |  | 3,3’-DMCHB** (%) | 3,3’-DMBP*** (%) | 4H-4,6-DMDBT**** (%) | Cracking Products (%) | Ratio Toluene / MCH |
| 0 | 0.628 | 86.3 | 5.8 | 0.7 | 7.2 | 1.08 |
| 0.02 | 0.483 | 84 | 9.4 | 1.3 | 5.3 | 1.11 |
| 0.04 | 0.288 | 82.3 | 8.9 | 1.9 | 6.9 | 1.16 |
| 0.08 | 0.108 | 50.1 | 2.4 | 2.9 | 44.5 | 1.21 |
| 0.20 | 0.174 | 58.2 | 8.4 | 3.9 | 29.6 | 1.34 |
| 0.32 | 0.269 | 56.8 | 7.0 | 4.7 | 31.5 | 1.46 |
| 0.49 | 0.133 | 51.8 | 5.8 | 3.9 | 38.6 | 1.53 |
| 0.61 | 0.204 | 57.9 | 7.3 | 1.9 | 32.9 | 1.47 |
| IRC | 0.831 | 88.4 | 11.3 | 0.3 | 0 | - |

* See the first footnote of Table 1.

** 3,3’-Dimethylcyclohexylbenzene. Including trace amounts of 3,3’-Dimethylbicyclohexyl (3,3’-DMBCH).

*** 3,3’-Dimethylbiphenyl.

**** Tetrahydro-4,6-dimethyldibenzothiophene. Including trace amounts of hexahydro-4,6-dimethyldibenzothiophene (6H-4,6-DMDBT) (less than an absolute value of ~ 0.2 %).