Table Captions

Table 1. Experimental conditions (variation of the temperature (T), the reaction time (t), and the [NaN3]0/[IC2H4C6F12C2H4I]0   initial molar ratio and yields of telechelic N3-C2H4-C6F12-C2H4-N3 diazido (B).

Table 2. Experimental conditions, yields, molecular weights, polydispersity indices (PDIs) and intrinsic viscosities of the polymers synthesized from the condensation of 1,10-diazido-1H,1H,2H,2H,9H,9H,10H,10H–perfluorodecane (B) with α,ω-dipropargyl ether bisphenol AF (A).

| Entry | T (°C) | t (hr) | [NaN3]0/[IC2H4C6F12C2H4I]0 | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | RT | 96 | 3 | 30 |
| 2 | RT | 96 | 6 | 40 |
| 3 | 50 | 48 | 3 | > 95 |

Table 1. Experimental conditions (variation of the temperature (T), the reaction time (t), and the [NaN3]0/[IC2H4C6F12C2H4I]0   initial molar ratio and yields of telechelic N3-C2H4-C6F12-C2H4-N3 diazido (B).

| Exp. | A / B / CuBr / bpy (mmol)a | r | Atmosphere | Yield (%) | Mnb (g/mol) | PDI | [η 35°C ]c (dL.g-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 4.94/5.10/0.40/0.80 | 0.97d | N2/O2 Traces | 60 | 37,000 | 1.8 | 0.4 |
| 2 | 1.21/1.20/0.40/0.80 | 0.99e | N2/ O2 Traces | 65 | 50,000 to >200,000 | 5.3 | 0.6 |
| 3 | 1.20/0.00/0.40/0.80 | - | N2/ O2 Traces | 43 | 5000 to 40,000 | 1.8 | - |
| 4 | 1.21/1.20/0.40/0.80 | 0.99e | O2 | 60 | 60,000 | 1.8 | 0.4 |

a A: n α,ω-dipropargyl ether bisphenol AF, B: n1,10-diazido1H,1H,2H,2H,9H,9H,10H,10H-perfluorodecane

b Mn assessed by SEC (Polystyrene standards)

c Intrinsic viscosity assessed in acetone at 35 °C

d r = A/B

e r = B/A

Table 2. Experimental conditions, yields, molecular weights, polydispersity indices (PDIs) and intrinsic viscosities of the polymers synthesized from the condensation of 1,10-diazido-1H,1H,2H,2H,9H,9H,10H,10H–perfluorodecane (B) with α,ω-dipropargyl ether bisphenol AF (A).