## Slide 1: Advanced approach to local magnetic field computation in magnetocaloric materials characterization
PhD student M. ALMANZA, Post-doc A. RAMINOSA, director A. Lebouc, S. Miraglia
UMR CNRS 5269 - Grenoble-INP – Université Joseph Fourier
Notes: The necessity for numerical simulation of magnetic cooling system to have intrinsec property of materials, lead us to this studies.
The aim is to obtain the magnetic curve B(H) through an extraction magnetometer with an error estimation.
And because it’s a intrinsic property the result must be independant of the shape.

## Slide 2: Quick reminder of Extraction Magnetometer
I . Intro
Measure of magnetic moment project on Z
isotropy on the material
symetries on the sample
And
Homogeneous material
because heterogeneity of H and
Notes: Just a quick reminder of extraction magnetometer
But it is not a system inversible because of the scalar product
With hypothesis of … we can expect to have an inversible system
But we can not

## Slide 3: Applied Field & Internal Field
I . Intro
Difference between applied field and the internal field
The gray volume feels :
the applied field
The field induce by the magnetization of its neighbours
Notes: Therefore

## Slide 4: Applied Field & Internal Field
I . Intro
Difference between applied field and the internal Field
Helmholtz decomposition
We define
Demagnetizing field respect
Notes: - Magnetic scalar potential
- In this part we show inhomogenity induce by the demag. Field and the demag. Field are not easy to compute in order to get the magnetic property of the measured sample because we have multiple interaction in the sample

## Slide 5: Advanced approach in magnetocaloric materials characterization
Introduction of the demagnetizing field and the heterogeneity
Demagnetizing Factor
Formulation as an inverse Problem
Demagnetizing Factor as an inverse problem
Perspectives
Notes: In some case the cope with the effect of demagnetizing field by using the notion of demag. factor

## Slide 6: Demagnetizing Factor
In elliptical shape
  The magnetic field is constant inside the body
  The demagnetizing field can be write as ith N only function of the geometry
  But experimentaly it is difficult to have elliptical shape
I. Intro > II. Demag. Factor
Notes: Voir si il y a des cas plus générales

## Slide 7: Generalization of the demagnetizing Factor
In general shape
  1st The field is not constant inside the body
  2nd extention of the notion of demagnetizing field define as:
  3rd approximation
  Approximations are difficult to validate
I. Intro > II. Demag. Factor
<
With N function of the geometry and
Notes: In this case we have many approximation that are very hard to justify to explain

## Slide 8: Test of the method
Test the method based on numerical simulation
Numerical setup
  Cylinder shape with radius 20 and = [5, 10, …,55]
  Generalized demagnetizing factor interpolated from D.X Chen table* But it is difficult to choose with non linear material
  Magnetization curve give by arctan. model with and
I. Intro > II. Demag. Factor
Magnetization ~ Gd
Simulation FEM
Compute
1st strategy : use of generalized demagnetizing factor
Comparaison
Analyse the Homogeneity of the field
Magnetometer simulation
Estimation
*D.-X. Chen, J. A. Brug, et R. B. Goldfarb, « Demagnetizing factors for cylinders », IEEE Transactions on Magnetics, vol. 27, no 4, p. 3601 ‑3619, juill. 1991.

## Slide 9: Result of the simulation
Homogeneity of the field
I. Intro > II. Demag. Factor
Magnetization volumic density normalized
Normalized error
Error of the method
A long sample improve the efficiency of the method
  Because the demagnetizing field decrease
Error between and his estimation
Notes: Even though
Bend part of the curve

## Slide 10: Advanced approach in magnetocaloric materials characterization
Introduction of the demagnetizing field and the heterogeneity
Demagnetizing Factor
Formulation as an inverse Problem
Demagnetizing Factor as an inverse problem
Perpectives

## Slide 11: Inverse problem
Scheme of the inverse problem and method of resolution
How to parametrize the magnetic curve « an unknown curve »
  With the previous test of the method we obtained anl error equal to zero with 3 parameters models because the magnetization is defined with the same model
Magnetization ~ Gd
Extraction
Compute
Simulation for inverse problem resolution
I. Intro > II. Demag. Factor > III. Inv. formulation
Magnetization ~ Gd
Simulation FEM
Mesure
Field distribution
Magnetometer experiment
Error
Evolution of parameters (of the magnetic curve)
Iterative loop

## Slide 12: How to parametrize the magnetic curve for the inverse problem
Generalized demagnetizing factor
Parametric function
  Model with 3 parameters
  Model with 4 parameters and avec
Parametric point (interpolated)
  Linear, Cubic, Spline interpolation
I. Intro > II. Demag. Factor > III. Inv. formulation
Complexity
Computation time
Degree of freedom
1
3
4
5 to
Notes: Computation time could be very long fonction of the geometry, of the mesh, solver and so on

## Slide 13: Advanced approach in magnetocaloric materials characterization
Introduction of the demagnetizing field and the heterogeneity
Demagnetizing Factor
Formulation as an inverse Problem
Generalized demagnetizing Factor as an inverse problem
Perpectives

## Slide 14: Prismatic sample in the magnetometer
Applied field
Magnetic moment
Gd prismatic sample 1x2x6 mm
I. Intro > II. Demag. Factor > III. Inv. Formulation > IV. Prismatic sample
Orientation ++
Orientation +++
Notes: Electric discharge machining, Length, longest

## Slide 15: Inversion based magnetometer mesurement
I. Intro > II. Demag. Factor > III. Inv. Formulation > IV. Prismatic sample
External Field
Relative error
External Field
Relative error
Temperature in K
Temperature in K
Error on the magnetic moment
Error on the magnetic moment
Demag. factor function of temperature for orientation +++
Error on the magnetic moment
Demag. factor function of temperature for orientation ++
Notes: Now we do the resolution of the inverse problem
Even though
Convergence criterion

## Slide 16: V. Perspectives
Method of comparaison
  Error on the magnetic moment
  B(H) should be the same for any shape
  Anistropie from process or Gd
  Use of cubic sample
Now we use parametric function and interpolated point
  To have a best fit of the magnetization curve to reduce the error NOW less than 0.5% on the magnetic curve (2h for one curve)
  Try to have an error estimation on the magnetization curve
Now we start to propagate the errors on
  Propagate the error througth the Maxwell Relation to have an estimation on the errors on the (intrinsec)
I. Intro > II. Demag. Factor > III. Inv. Formulation > IV. Prismatic sample > V. Perspectives
Magnetization M
Magnetization curve at 283 K

## Slide 17
Thanks for your attention
Question ?
By morgan.almanza@g2elab.grenoble-inp.fr