## Slide 1: Modeling the filtration of deformable and permeable colloidal particles: the case of casein micelles Peng Qu*, Antoine Bouchoux, Geneviève Gésan-Guiziou
INRA - French National Institute of Agricultural Research Agrocampus Ouest
UMR1253 STLO, Science and Technology of Milk and Egg, F-35000 Rennes, France
1
GDR AMC2 2011
Toulouse
13-14 October, 2011

## Slide 2: 1. Context
Dead-end filtration of colloidal particles
3
 A single equation to describe concentration polarisation and deposit layers
Diffusion and convection
in a polarised layer
Compression and permeation
in a deposit
2
x
J
With
D0 individual diffusion coefficient
K(f) sedimentation coefficient
k(f)  permeability
P  osmotic pressure
f  volume fraction
D(f)  collective diffusion coefficient
[Bacchin, Gordon Research Conference Membranes,2006]

## Slide 3
3
Happel equation
Filtration model for non-interacting hard spheres
Carnahan-Starling equation
1. Context
3
DP
Permeability
Osmotic pressure

## Slide 4
4
Filtration model for charged hard spheres
1. Context
[Bacchin et al., Desalination, 2006]
Experimental measurements
4
DP
Happel equation
Permeability
Osmotic pressure
(Latex)

## Slide 5
Filtration model for compressible and/or permeable particles
2. Research questions
5
Experimental measurements
Permeability
Osmotic pressure
Happel equation
Emulsion
Micro-gels
Casein micelles

## Slide 6
Filtration model for compressible and/or permeable particles
2. Research questions
6
Permeability
Osmotic pressure
Happel equation
Cheese production & proteins fractionation
Why milk filtration ?
~80% of the proteins in milk
Casein micelles
[Bouchoux et al., Biophys. J., 2009]
= Colloidal object (≈ sphere) :
Size distribution ~50-500nm
Water content 3.7g water/g proteins

## Slide 7
Filtration model for compressible and/or permeable particles
2. Research questions
7
Permeability
Osmotic pressure
Happel equation
Casein micelles
[Bouchoux et al., Biophys. J., 2009]
- How to determine the permeability?

## Slide 8
8
3. Measurement of permeability: strategy 1
Using osmotic stress
J0
e
DP=DP e=Vgel/Asac
Jt
P
P + DP
mgel
t
J0
P
P + DP

## Slide 9
Using the model “reversely”
[Bowen et Williams, J. Coll. Int. Sci., 2001]
9
[Bouchoux et al., Biophys. J., 2009]
Model validation:
Can we use the results for the prediction of filtration in any other conditions?
Permeability
Osmotic pressure
3. Measurement of permeability: strategy 2

## Slide 10
10
4. Permeability of casein micelles
The results are continuous and homogeneous
The results determined by the two methods are similar

## Slide 11
11
Phase transition (close packing) limits permeability
close packing
Permeability values = 2 regimes
4. Permeability of casein micelles

## Slide 12
12
Very different from the “monodispersed hard spheres”
Regime 1 - Before close packing
rp=50nm
close packing
4. Permeability of casein micelles

## Slide 13
13
The difference is not due to the polydispersity
It should not be due to the porosity of micelles
 dispersions of porous particles are supposed to be more permeable than dispersions
of hard particles [Adade, JCP, 2010]
[McMahon et Oommen, J. Dairy. Sci., 2008]
Regime 1 - Before close packing
[Li et Park., Ind. Chem. Res., 1998]
close packing
4. Permeability of casein micelles
Other effects (proteins residual from proteolyses of micelles ) affect the measurement?  work in progress…

## Slide 14
14
rp=4.5nm
Casein micelles ≈ bags of small spheres
Regime 2 - After close packing
After close packing:
close packing
4. Permeability of casein micelles
How does the internal organization of casein micelles affect the permeability ?

## Slide 15
5. Permeability of modified casein micelles
Effect of NaCl 100mM
Osmotic pressure
Filtration experiments
[Bouchoux et al., Biophys. J., 2009]
14
15
Ca2+ Na+
SAXS: void region ↓
Casein micelles

## Slide 16
5. Permeability of modified casein micelles
180-350 g/L, permeability is limited by the addition of 100mM NaCl
 More tortuous or less porous structure
>350 g/L, the permeabilities of the two dispersions become similar
Effect of NaCl 100mM
close packing
16

## Slide 17
5. Permeability of modified casein micelles
Sodium Caseinate
Osmotic pressure
Filtration experiments
[Bouchoux et al., Biophys. J., 2009]
Casein micelles
Sodium caseinate
17

## Slide 18
5. Permeability of modified casein micelles
150-350 g/L, sodium caseinate dispersion is less permeable
Sodium Caseinate
close packing
18
Casein micelles
Sodium caseinate
 More tortuous or less porous structure
>350 g/L, the permeabilities of the two dispersions become similar

## Slide 19
5. Permeability of modified casein micelles
After close packing: the permeability is limited while the salt is added or the micelles
are dissociate
 More tortuous or less porous structure
>350 g/L, the permeability is less dependent of the different conditions
 Whatever its initial structure, the system becomes homogeneous when it is highly packed
close packing
19

## Slide 20
6. Model validation
20
[Bouchoux et al., Biophys. J., 2009]
Permeability
Osmotic pressure
Prediction is possible

## Slide 21
[David et al.,Langmuir, 2008]
21
Prediction vs. experimental results
The results are satisfying and encouraging
6. Model validation

## Slide 22
7. Conclusion
In the future…
Continue to understand how the permeability is affected by the organization of
casein molecules in the micelles? What are the consequences on the filtration?
pH? Internal cross linking by enzyme?...
22
1. We determined the permeability of dispersions of permeable and
compressible colloids
3. Able to predict the filtration of soft objects – General model for colloids
2 regimes = before and after close-packing
2. Casein micelles are individually permeable, the permeability can be limited
while the salt is added or the micelles are dissociated.

## Slide 23: Thank you.
23
Thanks to Mr. Patrice Bacchin.