## Slide 1: Viscoelasticity of Supramolecular Center-functionalized Polymer
Xavier Callies
Effect of the strength of Hydrogen Bonding Stickers
Costantino Creton, Guylaine Ducouret
AERC 2015 - Nantes

## Slide 2
Supramolecular Polymers ?
Supramolecular Chemistry
Lehn, J. Angew. Chem.-Int. Ed. Engl. 1990, 29, 1304–1319.
Self-assembly of small molecules by non covalent bonds (H-bonds, ionic…) in solution
2

## Slide 3
Supramolecular Polymers ?
Supramolecular Chemistry
Polymer Physics
Association by covalent bonds of monomers
Rubinstein, M.; Colby, R. H. Polymer Physics; Oxford University Press, 2003.
Lehn, J. Angew. Chem.-Int. Ed. Engl. 1990, 29, 1304–1319.
Self-assembly of small molecules by non covalent bonds (H-bonds, ionic…) in solution
2

## Slide 4
Supramolecular Polymers ?
Supramolecular Chemistry
Polymer Physics
Supramolecular
Polymers
Association by covalent bonds of monomers
Rubinstein, M.; Colby, R. H. Polymer Physics; Oxford University Press, 2003.
Lehn, J. Angew. Chem.-Int. Ed. Engl. 1990, 29, 1304–1319.
Self-assembly of small molecules by non covalent bonds (H-bonds, ionic…) in solution
2

## Slide 5
Interactions
between Stickers
Interest of Supramolecular Polymers ?
Specific
Reversible
Clusters, Aggregates, Networks
or Nanostructures
Strong dependency with their environment
3

## Slide 6
Interest of Supramolecular Polymers ?
UV (Heat)
Stimuli-responsive
Materials
Self-healing
by simple contact at RT
Fracture
Healing
Heinzmann, C. et al,
ACS Appl. Mater. Inter.
2014, 6,4713–4719.
Cordier, P. et al, Nature 2008, 451, 977–980.
3
A wide diversity of applications
Interactions
between Stickers
Specific
Reversible
Clusters, Aggregates, Networks
or Nanostructures
Strong dependency with their environment

## Slide 7
What is the effect of the strength of stickers on the rheological behavior ?
How to link the rheological properties and the chemical structure of the polymer chain ?
Challenge for all applications
4
+
ka
kd
Strength of Stickers
K = ka / kd
ΔH
Chemistry of stickers
Polarity of Polymer Matrix
Notes: This question was a difficult one because you take this dynamics into account….

## Slide 8
Poly(butylacrylate)
Copolymers
Lewis et al, Macromolecules, 2014, 47, 729–740.
5
Weak
Stickers
Strong
Stickers
or
or
Background

## Slide 9
Poly(butylacrylate)
Copolymers
5
or
Weak
Stickers
Strong
Stickers
”Tg effect”
”Tg effect” +
supramolecular
network
or
Weak
Stickers
Strong
Stickers
Lewis et al, Macromolecules, 2014, 47, 729–740.
Background

## Slide 10
6
Center-functionalized Polymers ?
Self-assembly of stickers
into filaments is favored
Predictable shape
of the aggregates
Link the rheology and
the supramolecular Chemistry
Frauenrath, H. et al. Chem. Sci. 3, 1512-1521 (2012)
Bouteiller, L. et al.. Adv. Funct. Mater. 20, 1803–1811 (2010).

## Slide 11
6
Center-functionalized Polymers ?
Strategy of our Project
Synthesis of monodisperse and linear center-functionalized polymers
Systematic characterization of the nanostructure and linear rheology.
Change the molecular parameters in a highly controlled way
Self-assembly of stickers
into filaments is favored
Frauenrath, H. et al. Chem. Sci. 3, 1512-1521 (2012)
Bouteiller, L. et al.. Adv. Funct. Mater. 20, 1803–1811 (2010).
Predictable shape
of the aggregates
Link the rheology and
the supramolecular Chemistry

## Slide 12
Tri-Urea Toluene
”Strong Sticker”
Bis-urea Xylene
”Weak Sticker”
Key-molecular parameters
7
1. Level of interactions : Two hydrogen bonding stickers.

## Slide 13
1. Level of interactions : Two hydrogen bonding stickers.
2. the interacting moieties density : the size of the linear non polar chains
Tri-Urea Toluene
”Strong Sticker”
Bis-urea Xylene
”Weak Sticker”
5 kg/mol ≤ Mw ≤ 100 kg/mol
4% ≥ Sticker (w%) ≥ 0,2%
PnBA
Key-molecular parameters
7
Ip ≤ 1,4

## Slide 14
2. the interacting moieties density : the size of the linear non polar chains
Tri-Urea Toluene
”Strong Sticker”
Bis-urea Xylene
”Weak Sticker”
5 kg/mol ≤ Mw ≤ 100 kg/mol
4% ≥ Sticker (w%) ≥ 0,2%
PnBA
Key-molecular parameters
7
Ip ≤ 1,4
1srt Part
2nd Part
1. Level of interactions : Two hydrogen bonding stickers.

## Slide 15
No variation of Tg with Mn (between 5 and 100kg/mol): Tg = -49 ± 1°C (DSC)
8
Tg and Nanostructure for Strong Stickers

## Slide 16
No variation of Tg with Mn (between 5 and 100kg/mol): Tg = -49 ± 1°C (DSC)
0,2
0,6
1,0
1,4
q (nm-1)
I (u.a)
5kg/mol
8kg/mol
No peak for Mn ≥ 40 kg/mol
23kg/mol
8
Tg and Nanostructure for Strong Stickers
SAXS Investigation

## Slide 17
No variation of Tg with Mn (between 5 and 100kg/mol): Tg = -49 ± 1°C (DSC)
0,2
0,6
1,0
1,4
q (nm-1)
I (u.a)
5kg/mol
8kg/mol
No peak for Mn ≥ 40 kg/mol
23kg/mol
8
Tg and Nanostructure for Strong Stickers
Oriented
Filaments
Randomly
Oriented Rods
SAXS Investigation
Mn ≤ 40 kg/mol
Self-assembly of
stickers
into filaments
Mn ≥ 40 kg/mol

## Slide 18
× 1
× 0,5
× 1,6
Rheology for Strong Stickers
5kg/mol
20kg/mol
60kg/mol
9

## Slide 19
Oriented
Filaments
Randomly
Oriented Rods
Dissipative
Gel
Mn ≤ 40kg/mol
Mn ≥ 40kg/mol
Viscoelastic
Fluid
Rheology for Strong Stickers
× 1
× 0,5
× 1,6
5kg/mol
20kg/mol
60kg/mol
9

## Slide 20
Shifts
« Frozen » Aggregates
Dissipative Relaxation
of the side chains
10
× 1
× 0,5
× 1,6
5kg/mol
20kg/mol
60kg/mol

## Slide 21
G’’ ≥ G’
ω ≠ f(Mw)
≈ 0,5
G’’ ≤ G’
11
× 1
× 0,5
× 1,6
5kg/mol
20kg/mol
60kg/mol

## Slide 22
Rouse / Entanglements
Tg
Gel / Fluid
Polymer Matrix
Self-assembly of Stickers
G’’ ≥ G’
ω ≠ f(Mw)
≈ 0,5
G’’ ≤ G’
Comb-shaped Aggregates
≈
Comb-shaped Polymers
11
× 1
× 0,5
× 1,6
5kg/mol
20kg/mol
60kg/mol

## Slide 23
12
Strong Stickers vs Weak Stickers ?
Molecular weight dependency ?

## Slide 24
η* (1rad/s, T=25°C)
Entanglements’ Regime
Mn ≥ Mc
Stickers’ Regime
Mn ≤ Mc
12
Strong Stickers vs Weak Stickers ?
Molecular weight dependency ?
Jullian, N.; Leonardi, F.; Grassl, B.; Peyrelasse, J.; Derail, C. Appl. Rheol. 2010, 20, 33685.
Critical Molecular weight (Mc) ?
Strong
Weak
PnBA

## Slide 25
η* (1rad/s, T=25°C)
Entanglements’ Regime
Mn ≥ Mc
Stickers’ Regime
Mn ≤ Mc
Strength ↗, Mc ↗
12
Strong Stickers vs Weak Stickers ?
Molecular weight dependency ?
Jullian, N.; Leonardi, F.; Grassl, B.; Peyrelasse, J.; Derail, C. Appl. Rheol. 2010, 20, 33685.
Critical Molecular weight (Mc) ?
Mc ≈ 40kg/mol
Mc ≈ 20kg/mol
Strong
Weak
PnBA

## Slide 26
Strong Stickers vs Weak Stickers ?
Stability of the nanostructure (below Mc) ?
13
Mn = 5kg/mol
Strong Sticker

## Slide 27
13
Strong Stickers vs Weak Stickers ?
Stability of the nanostructure (below Mc) ?
Strong Sticker
Mn = 5kg/mol
Weak Sticker

## Slide 28
13
Strong Stickers vs Weak Stickers ?
Stability of the nanostructure (below Mc) ?
Mn = 5kg/mol
Strong Sticker
Weak Sticker
T ≤ TODT
T ≥ TODT

## Slide 29
Frozen Structure over a long distance range
Gel plateau
T ≤ TODT
13
Strong Stickers vs Weak Stickers ?
Stability of the nanostructure (below Mc) ?
Scission / Association of Stickers
Viscoelastic Fluids
T ≥ TODT
Mn = 5kg/mol
Strong Sticker
Weak Sticker

## Slide 30
Conclusion on linear rheology of center-functionalized Polymers
G’
G’’
Monomer
Friction
Entanglement
/ Rouse
Gel
/ Fluid
ω
14

## Slide 31
Conclusion on linear rheology of center-functionalized Polymers
Fine Control of the viscoelasticity via the chemical structure
G’
G’’
ω
Monomer
Friction
Entanglement
/ Rouse
Gel
/ Fluid
Density and Strength of Stickers
TODT and Mc
14

## Slide 32: Thank you for all People in Project ANR SUPRADHESION
Cécile Fonteneau
Sandrine Pensec, Laurent Bouteiller
Jean-Marc Chenal, Laurent Chazeau
Cyril Véchambre
Guylaine Ducouret
Costantino Creton

## Slide 33
Thank you for your attention !