## Slide 1: Biaxial Testing of Knitted NiTi Textiles: DIC VS Adapted Image Processing
N. Connesson*, F. Tissot † , D. Favier*, L. Heller‡
‡Institute of Physics, Prague, Czech Republic
*Laboratoire TIMC, Grenoble, France

## Slide 2: Introduction
L. Heller, ‡Institute of Physics, Prague, Czech Republic
NiTi Knitted textile (φ 100 µm)

## Slide 3: Introduction
L. Heller, ‡Institute of Physics, Prague, Czech Republic
NiTi Knitted textile (φ 100 µm)
Mechanical behaviour
???
Biaxial testing

## Slide 4: Introduction
Grips and
Force transducer
Camera
Biaxial testing

## Slide 5: Introduction
Anisotropy
Harmonic main load
Harmonic main load
Displacement
Biaxial testing
Extract data from the pictures …

## Slide 6: Introduction
Harmonic main load
Data we would like to extract :
Displacement fields
  => Strain fields
And… :
  Geometria of wire/loops
  Gliding => energy dissipation by friction

## Slide 7: Introduction
How to extract these data ?
DIC VS Adapted Image Processing
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 8: Outline
Introduction
  I. DIC
  II. Data Processing
    Displacements fields
    Shape and gliding
Conclusion

## Slide 9: Outline
Introduction
  I. DIC
  II. Data Processing
    Displacements fields
    Shape and gliding
Conclusion

## Slide 10: I. DIC
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
2D Digital Image Corrélation (Vic 2D)
Immaterial points tracking => lack physical meaning 
Not an optimal speckle…

## Slide 11: I. DIC
Can we do better ?
Well, yes !

## Slide 12: Outline
Introduction
  I. DIC
  II. Data Processing
    Displacement fields
    Shape and gliding
Conclusion

## Slide 13: II. Data Processing a) Displacement fields
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
Loop center identifcation
(Bwlabel, Matlab)
Loop center
=> more physical meaning 
=>
Knitted structure
Time tracking
=>

## Slide 14
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
Time tracking (Bwlabel, Matlab)
t0
Update position at t0 => position at t1
t1=t0+dt
  II. Data Processing a) Displacement fields

## Slide 15: II. Data Processing a) Displacement fields
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
t0
t1=t0+dt
Update position at t0 => position at t1
Time tracking (Bwlabel, Matlab)

## Slide 16: II. Data Processing a) Displacement fields
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
Home made data processing
DIC (Vic 2009)

## Slide 17: II. Data Processing
We exctracted :
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 18: Outline
Introduction
  I. DIC
  II. Data Processing
    Displacement fields
    Shape and gliding
Conclusion

## Slide 19: II. Data Processing b) Shape and gliding
Spoiler :
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 20: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 21: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
Bwlabel

## Slide 22: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
Bwlabel
Bwperim

## Slide 23: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 24: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 25: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 26: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 27: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 28: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 29: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 30: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 31: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 32: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 33: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 34: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 35: II. Data Processing b) Shape and gliding
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction

## Slide 36: Outline
Introduction
  I. DIC
  II. Data Processing
  III. Comparision
  IV. Further processing
Conclusion

## Slide 37: Conclusion
Displacement fields / Strain fields
Geometria of wire/loops
Gliding => energy dissipation by friction
DIC (Vic 2009)
Home made data processing

## Slide 38: The End

## Slide 40: Friction
Idée : Solide soumis à deux efforts

## Slide 41
Centre de gravité
Poids mg

## Slide 42
Centre de gravité
Poids mg

## Slide 44
Introduction : utilité
Langue de boeuf
//
┴
Non linear behavior
Anisotropy
Gipsa Lab collaboration (P. Perrier)
Utilisation possibles : en NiTi, c’est biocompatible !
Historiquement :
  Matériau architecturé,
  Tricots de métaux (acier, NiTi, etc)
Ludek Heller

## Slide 45
Results from tensile tests on tissue samples from oesophagus; Natali et al (2009)
Tensile test on artery; Chagnon et al (2012)
Introduction : utilité
Historiquement :
  Matériau architecturé,
  Tricots de métaux (acier, NiTi, etc)
Ludek Heller

## Slide 46
Introduction : utilité
Applications ?
Historiquement :
  Matériau architecturé,
  Tricots de métaux (acier, NiTi, etc)
Ludek Heller
…
Géométrie,
Diamètres,
Traitement thermiques
Shape setting
Paramètres :

## Slide 47: Analyse: Géométrie initiale
h
L
h
L
~ 135
~ 148
Cellule i
Position CdG,
4 Segments,
Intersections.

## Slide 48: Analyse: Géométrie initiale
largeur 1
largeur 2
largeur 1
largeur 2
Cellule i
Position CdG,
4 Segments,
Intersections.

## Slide 49: Analyse: Géométrie initiale
θ
Axe de symétrie (théorique)
α1
α2
Cellule i
Position CdG,
4 Segments,
Intersections.

## Slide 50: Approche numérique : Modèle EF
Fil NiTi (Ni-54wt%) : ø0,1 mm,
X: 4,35 mm / Y: 2,305 mm
Géométrie “moyenne” représentative (??)
Conditions limites: périodiques + déplacement
Modèle de matériau : Bilinéaire (Acier) ou Auricchio
Frottement sec (Expérience “maison’, ok)