## Slide 1: IR heating of green wood while peeling: a numerical model.
Plan:
The project idea
The model principles
The simulation results
Collaboration:
Louis-Etienne DENAUD1, Mark HUGHES2, Andrezj KUSIAK3, Rémy MARCHAL1, Sid’Ahmed OULD AHMEDOU1, Fréderic ROSSI1.
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu
1Arts et Métiers ParisTech LaBoMaP, France
3Université de Bordeaux, France
2Aalto University, Helsinki, Finland

## Slide 2: Peeling process: veneer production
Veneer
Soaking
Peeling
Pressure bar
Knife
e ± Δe
Plywood

## Slide 3: Why soaking?

## Slide 4: Alternative methods to heating wood prior to peeling avoiding soaking
Electric ohmic heating
Microwave
heater
Volume
heating
              Microwave heating
Infrared
heater
Wood does not need to be cooked for a long duration nor at boiling temperatures
Cell wall has to be brought at the required medium range temperature
Surface
heating
    Infrared heating (IR)
Electrode
U = 10 V/mm
Electrode

## Slide 5: Modelling in-line IR surface heating: principle
Bolt
IR
heater
Equations solver Comsol Multiphysics®
Procedure implemented under MatLab®
Maximum cutting speed?
Efficient wavelengths? Efficient power?
Without overheating bolt surface?
The answer here:
By numerical modelling of IR heating while peeling

## Slide 6: Methodology: meshing and sensitivity analysis
3

## Slide 7: Heat transfer equations
Chart: Emittance Mλ ( W/m3)
VISIBLE
INFRARED
ε wood emissivity (no dimension)
σ Stefan-Boltzmann constant (W.m-2.K-4)
Planck’s law
ρ wood density (kg.m-3)
Cp heat capacity of the wood (J.kg-1.K-1)
T bolt temperature (K)
k conductivity of wood (W.m-1.K-1)
Qrad external IR heat source
h heat transfer coefficient (W.m-2.K-1)
Text external IR source temperature (K)
(1)
(2)

## Slide 8: Subdomain settings
kg.m-3
Each Finite Element is parametered with wood physical properties, taking into account natural defects (knots, rays, off-centered pith)
Continuous peeling with a circle trajectory

## Slide 9: Boundary conditions
Bolt
IR
heater
Constant angle
Constant distance

## Slide 10: Temporal evolution of temperature within the bolt during one turn
Peeling speed = 0.1 m/s

## Slide 11: Influence of the distance between the knife and the IR source
IR source temperature Text = 2500°C
peeling speed v = 0.3 m/s

## Slide 12: Influence of peeling speeds and peeling thickness
IR source temperature Text = 500°C
Peeling thickness e = 1 mm

## Slide 13: Influence of peeling speeds and peeling thickness
IR source temperature Text = 500°C
Peeling thickness e = 2 mm

## Slide 14
To locate IR source as far as possible from the knife
FUTURE WORK
To integrate in the model:
green wood thermal properties : Cp, k = f(MC)
> with transient HotDisk®method (TREFLE, Bordeaux)
> should speed up heat penetration
green wood optical properties : emissivity, transmittivity, absorptivity = f(λ)
> modifying model’s equations with IR volumic Beer- Lamberts absorption law(CNRS, Orléans)
> should deepen radiation penetration
To experimentally validate the model
- to establish it as an essential decision-making tool to design in-line IR heating system directly embedded on the cutting machine
(1)
with
and
(2)
(s
CONCLUSIONS SO FAR ON THE OPTIMUM CONFIGURATION

## Slide 15: IR heating of green wood while peeling: a numerical model.
Baldwin, R.F., (1975) Plywood Manufacturing Practices. Miller Freeman Publications Inc., San Fransisco, California, pp 62-78.
Bardet, S., Beauchêne, J., Thibaut, B.,(2003) Influence of basic density and temperature on mechanical properties perpendicular to grain of ten wood tropical species. Annals of Forest Science. 60(1):49-59. Bedard, N., Laganiere, B., (2009) Debarking Enhancement of Frozen Logs. Part II: Infrared System for Heating Logs Prior to Debarking. Forest Products Journal. 59(6):25-30.
Coste, N., (2005) Interest of radiant energy for wood peeling and slicing process. Master's thesis, University of Melbourne.
Dupleix, A., Marchal, R., Bléron, L., Rossi, F., Hughes; M., (2011) On-line heating temperatures of green-wood prior to peeling. Joint International Symposium on Wood Composites and Veneer Processing and Products Proceedings.
Flir Systems (2004) ThermaCAM User's Manual.
Gaudilliere, C., (2003) Contribution au développement d’une chauffe électrique rapide de bois vert de Douglas en vue de son déroulage. Master's thesis, Arts et Métiers ParisTech.
Glass, S.V., Zelinka, S.L., (2010) Wood handbook, Chapter 04: Moisture relations and physical properties of wood. General Technical Report FPL-GTR-190 Department of Agriculture, Forest Service, Forest Products Laboratory, Madison, WI, US. 4-1 - 4-19.
Lutz, J.F., (1960) Heating veneer bolts to improve quality of douglas-fir plywood. Technical report USDA Forest Service General FPL-2182, Forest Products Laboratory, Madison, WI, US.
Marchal, R., Collet, R., (2000) Contribution au développement d'une chauffe électrique rapide de bois vert de douglas en vue de son déroulage. Technical report, Arts et Métiers ParisTech.
Marchal, R., Gaudilliere, C., Collet, R., (2004) Technical feasibility of an embedded wood heating device on the slicer or the peeling lathe. International Symposium Veneer Processing and Products Proceedings. pp 29-44.
Matsunaga, M., Minato, K., (1998) Physical and mechanical properties required for violin bow materials II: Comparison of the processing properties and durability between pernambuco and substitutable wood species. Journal of Wood Science. 44(2):142-146.
Potter, B.E., Andresen, J.A., (2010) A finite-difference model of temperatures and heat flow within a tree stem. Revue Canadienne de Recherche Forestière. 32(3):548-555.
Torgovnikov, G., Vinden, P., (2010) Microwave wood modification technology and its applications. Forest Products Journal. 60(2):173.
Yamauchi, S., Iijima, Y., Doi, S., (2005) Spectrochemical characterization by FT-Raman spectroscopy of wood heat-treated at low temperatures: Japanese larch and beech. Journal of Wood Science. 51(5):498-506.
Thank you for your attention
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu