## Slide 1: IR heating of green wood while peeling.
Collaboration:
Louis-Etienne DENAUD1, Mark HUGHES2, Andrezj KUSIAK3, Rémy MARCHAL1, Sid’Ahmed OULD AHMEDOU1, Fréderic ROSSI1.
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu
1Arts et Métiers ParisTech LaBoMaP, France
3Université de Bordeaux, France
2Aalto University, Helsinki, Finland

## Slide 2: IR heating of green wood while peeling.
Plan
The project idea
Heating temperatures
Modelling principles
Thermal characterisation results
Future work
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 3: IR heating of green wood while peeling.
1.The project idea
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 4: Peeling process: veneer production
Veneer
Soaking
Peeling
Pressure bar
Knife
e ± Δe
Plywood

## Slide 5: Why soaking?

## Slide 6: Alternative methods to heating wood prior to peeling avoiding soaking
Electric ohmic heating
Microwave
heater
Volume
heating
              Microwave heating
Infrared
heater
Wood does not need to be cooked for a long duration nor at boiling temperatures
Cell wall has to be brought at the required medium range temperature
Surface
heating
    Infrared heating (IR)
Electrode
U = 10 V/mm
Electrode

## Slide 7
Work in collaboration with : 1Post-doc S. Ould Ahmedou
2Master thesis G. Belluche
Technical feasibility
Values
Specifications
Requirements
Economical feasibility
Start
Conclusion
Economical study of embedded IR heating system
Modelling IR heat transfer during peeling process2
Validating tests on embedded IR heating system
Optimisation of IR heating parameters
Characterisation of wood behaviour under IR radiation1
Minimum required peeling T°C
Technical development of embedded IR heating system
Peeling unit
Thermal unit
Economical unit
Time

## Slide 8: IR heating of green wood while peeling.
2.Heating Temperatures
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 9: Results summary
No interest in heating up to 70°C
With heating temperatures:
- Cutting efforts start to decrease
- Lathe checkings are less deep and closer
- Minor thickness variation
Already at 50°C, positive effects of heating ensure efficient peeling process.

## Slide 10: IR heating of green wood while peeling.
3.Modelling results
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 11: Modelling in-line IR surface heating: principle
Bolt
IR
heater
Equations solver Comsol Multiphysics®
Procedure implemented under MatLab®
Maximum cutting speed?
Efficient wavelengths? Efficient power?
Without overheating bolt surface?
The answer here:
By numerical modelling of IR heating while peeling

## Slide 12
ρ wood density (kg.m-3)
Cp heat capacity of the wood (J.kg-1.K-1)
T bolt temperature (K)
k conductivity of wood (W.m-1.K-1)
Qrad external IR heat source
h heat transfer coefficient (W.m-2.K-1)
Text external IR source temperature (K)
(1)
(2)
Methodology: meshing and equations

## Slide 13
Simulation results
e=2mm
e=1mm
v=0.1m/s

## Slide 14: IR heating of green wood while peeling.
3.Thermal characterisation
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 15: The transient HotDisk method
At t0
High λ
Low λ
At t > t0
Low κ
High κ
Low Cp
High Cp
T(K)
0 K
Remaining
heat
Heat rate
T(K)
T+1(K)
Heat speed
T(K)
0 K
T(K)
0 K
T(K)
0 K
Low Cp
Heat storage
Conductivity λ
Diffusivity κ
Heat Capacity Cp

## Slide 16: Transversal conductivity

## Slide 17: Heat capacity

## Slide 18: Diffusivity

## Slide 19: IR heating of green wood while peeling
4. Future Work
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu

## Slide 20
Technical feasibility
Values
Specifications
Requirements
Economical feasibility
Start
Conclusion
Economical study of embedded IR heating system
Modelling IR heat transfer during peeling process2
Validating tests on embedded IR heating system
Optimisation of IR heating parameters
Characterisation of wood behaviour under IR radiation1
Minimum required peeling T°C
Technical development of embedded IR heating system
Peeling unit
Thermal unit
Economical unit
Time

## Slide 21
FUTURE WORK
To integrate in the model:
green wood thermal properties : Cp, k = f(MC)
> with transient HotDisk®method (TREFLE, Bordeaux)
> should speed up heat penetration
green wood optical properties : emissivity, transmittivity, absorptivity = f(λ)
> modifying model’s equations with IR volumic Beer- Lamberts absorption law(CNRS, Orléans)
> should deepen radiation penetration
To experimentally validate the model
to establish it as an essential decision-making tool to design in-line IR heating system directly embedded on the cutting machine
To study the economical feasibility of the project
(1)
with
and
(2)
(s

## Slide 22: IR heating of green wood while peeling.
Thank you for your attention
Anna DUPLEIX – PhD Candidate
anna.dupleix@ensam.eu