## Slide 1: Feasibility of wood peeling process assisted by radiant energy.
Anna DUPLEIX
PhD student – First year
1Arts&Métiers ParisTech Cluny, France; 2Aalto University, Helsinki, Finland ; 3Université de Bordeaux, France.
Professor Rémy MARCHAL1
Professor Mark HUGHES2
Joint supervisors: Dr Louis-Etienne DENAUD1
Dr Andrezj KUSIAK3
Dr Fréderic Rossi1

## Slide 2: A high-value added process. A high production rate.
Slow down by log preparation.
Peeling process1
Thickness =0.5 to 10 mm
v =1 to 10 m/s
Sources: 1CarterHoltHarvey WoodProducts New Zealand; 2Bois Déroulés de l’Auxois.
Soaking
24-72 h
Time of process
Peeling
1 min
2

## Slide 3: What is wood heating prior to peeling aimed at?
To « soften » wood prior to peeling.
Sources: 3P.Navi Traitement hyggrothemro du bois, 4SMOF.
to fluidise resin pockets
to soften lignin and knots
to facilitate peeling of shavings
to reduce the risk of lathe checkings
Lowering cutting efforts
to increase wood deformability
to reduce applied power
to limitate wear of the cutting tools
B = tight side
A = loose side
Open lathe checkings4
Improving veneer surface quality deformability
SMOF setup4

## Slide 4: Soaking: a traditional method
Sources: 5Baldwin, 1981; 6Bois Déroulés de l’Auxois; 7 Arts&Métiers ParisTech Cluny.
Aim of soaking: To heat bolts in the whole volume.
Cost | Yield | Veneer quality
Energy efficiency Water pollution Facilities requirements | Stock downtimes Wood cohesion Handling | Coloration Durability Wooly surface
Severe drawbacks in terms of
5;6
Chart: 
| Beech | Douglas
Soaking Temperature | 70 | 60
Soaking Duration | 30 | 48
But time-consuming, empirical and imperfect.
7

## Slide 5: Previous trials on alternative methods to soaking Arts et Métiers ParisTech Cluny
To heat wood prior to peeling.
Electric ohmic heating
    Microwave heating (MW)
Electrodes insulated with Teflon®
Temperature sensors
Scale
Bolt
8
Microwave
heater
9
Infrared
heater
10
Sources: 8,10 Arts&Métiers ParisTech Cluny; 9University of Melbourne.
Volume
heating
Surface
heating
    Infrared heating (IR)

## Slide 6: For same veneer quality, a high heating rate method.
But heterogeneous and requiring high voltages.
V/mm
°C/min
Sapwood
°C/min
V/mm
Heartwood
Electrode
Electrode
U = 10 V/mm
Current flows mainly in sapwood
Sources: 11 Marchal, R. et al., 2000-2004.
11
Chart: Heating rates comparison of electric ohmic and soaking methods
| Electric ohmic Sapwood | Electric ohmic Heartwood | Soaking
 | 5 | 3.5 | 0.1
Volume
heating

## Slide 7: Learning from volume electric ohmic heating.
Wood does not need to be "cooked" to "soften" as required by peeling.
Using water as vector of heat produces heterogeneous heating.
1
2
How to heat wood without using water as a vector of heat?
Chart: Hygrometry of Douglas-fir bolts after soaking (48h, 60 °C)
| 0 | 0.61613576839826867 | 1.2322715367965413 | 1.8484073051948031 | 2.4645430735930667 | 3.0806788419913445 | 3.6968146103895987 | 4.3129503787878418 | 4.9290861471861325 | 5.6759432900432731 | 6.4228004329004085 | 7.1696575757575545 | 7.916514718614696 | 8.6633718614717861 | 9.4102290043289774 | 10.157086147186122 | 10.903943290043276 | 11.6508004329004 | 12.397657575757552 | 13.144514718614682 | 13.891371861471772 | 14.638229004328963 | 15.385086147186152
 | 36.2705 | 37.4768 | 37.1771 | 38.5081 | 40.3023 | 41.4716 | 41.9149 | 43.7956 | 43.4911 | 40.6417 | 77.8656 | 54.8485 | 103.7109 | 43.1193 | 49.1607 | 125.5259 | 43.6937 | 90.5141 | 91.2281 | 54.111 | 65.3672 | 82.1869 | 115.8981
 | 0 | 200
heartwood
sapwood

## Slide 8: Interest of radiant energy
Chart: Emittance Mλ ( W/m3)
Energy efficiency
Planck’s law
Radiation penetrates into green wood
VISIBLE
INFRARED

## Slide 9: Homogeneous and rapid heating but dangerous.
Looking for radiant energy heating easier to implement.
Coaxial cables and waveguides from electric generator to MW applicator.
12
13
Sources: 12 Torgonikov et al., 2010; 13University of Melbourne.
Chart: Log under MW heating (12 kW)
| 60 | 40 | 0
Probe 60 mm | 110 | 100 | 20
MW
60 mm
Probe
Log
Chart: Comparison of heating rates to heartwood of MW and electric ohmic methods
| Microwave | Electric Ohmic
 | 2.5 | 0.066667
MW Volume
heating

## Slide 10: IR thermal kinectics
Surface layer
IR penetration
Conduction
Subjacent layers
Rapid surface heating.
0 10 20 30 40 Time (s)
Temperature (°C)
Chart: Heating rates comparison of IR and MW to reach 80 °C
| Infrared Surface | Infrared 0,5 mm | Infrared 3 mm | Microwave
 | 16 | 10.6667 | 0.59259 | 0.041667
140
120
100
80
60
40
20
0
14
Sources: 14 CETIAT, 2003.
IR Surface
heating

## Slide 11: Alternative methods to soaking
IR most suitable alternative method to heat wood prior to peeling.
 | Advantages | Drawbacks
Electric ohmic heating | - rapidity | - requiring high voltages
Microwave heating | - rapidity - energy efficiency | - complexity of technology
Infrared heating | rapidity - easiness of implementation | - penetration depth

## Slide 12: Aim of research: to develop on-line IR heating system
directly embedded on the peeling lathe
to heat wood surface while peeling
activated when peeling comes to heartwood
Bolt
Peeling knife
IR radiation
IR radiation

## Slide 13
70°C 60°C 50°C 45°C 40°C 35°C 30°C 20°C
Heating bolts by soaking
Process parameters
V = 1 m/s
Bp = 5%
e = 3 mm
Study of the influence of heating temperatures on peeling.
Objectives To lower heating temperatures in compromise with veneer surface quality.
Results Target temperatures for modelling.
Species
Douglas-fir
Beech
Spruce
Birch
Process assessment
On-line surface temperatures (IR camera) Cutting efforts on pressure bar Moisture Content cartography of bolt
Veneer quality assessment
Checks index (fuitometer)
Veneer thickness
Checks frequency and depth (SMOF)
e ± Δe

## Slide 14
Technical feasibility
Values
Specifications
Requirements
Economical feasibility
Start
Conclusion
Economical study of embedded IR heating system
Modelling IR heat transfer during peeling process
Validating tests on embedded IR heating system
Optimisation of IR heating parameters
Characterisation of wood behaviour under IR radiation
Minimum required peeling T°C
Technical development of embedded IR heating system
Peeling unit
Thermal unit
Economical unit
Current work
Time
Post-doc
S. Ould Amadou

## Slide 15: Feasibility of wood peeling process assisted by radiant energy.
Thank you for your attention.
Professor Rémy MARCHAL
Arts&Métiers ParisTech Cluny, France
Professor Mark HUGHES
Aalto University, Helsinki, Finland
Anna DUPLEIX
PhD student – October 2010