## Slide 1: Future MTR capabilities : Jules Horowitz Reactor
Jean-François VILLARD, Gilles BIGNAN
French alternative energies and atomic energy commission
Nuclear Energy Division – Reactor Studies Department
Cadarache – F-13108 St Paul Lez Durance, France
Joint ICTP/IAEA Workshop “Research Reactors for Development of Materials and Fuels for Innovative Nuclear Energy Systems”
6-10 November 2017, ICTP - Trieste, Italy

## Slide 2: Future MTR capabilities : Jules Horowitz Reactor
Summary
Context and objectives of the JHR
General figures of the JHR
Experimental capabilities of the JHR
The key-role of innovative instrumentation for the JHR
JHR consortium and collaborations
PAGE 2

## Slide 3: 1. Context and objectives of the JHR

## Slide 4: 1. Context and objectives of the JHR
In-pile testing in support of the nuclear Industry
Just for France, 58 NPPs means more than 10 000 fuel assemblies under irradiation at a time…
The fuel has to be carefully designed, with enough Safety Analysis Design Margins
+ new fuel managements
+ new LWR standards…
In-pile data required !
 need to generate additional margins
  Improve Modeling, Calculation tools and Testing
  Improve Safety Analysis design Methods
  Improve Fuel Product

## Slide 5: 1. Context and objectives of the JHR
The Key-Role of Material Testing Reactors for Fuel and Material qualification under irradiation
BASIS RESEARCH
&
NUMERICAL SIMULATION
SINGLE EFFECT
EXPERIMENTS
POST IRRADIATION
EXAMINATIONS
MANUFACTURING
REFABRICATION
CHARACTERIZATION
BEHAVIOUR UNDER IRRADIATION
Material Test Reactor
Hot Lab.
EXPERIMENTAL DATA
EXPERTISE
Hot lab. for PIE
CODES
Validation
QUALIFICATION
Documents
CEA
DESIGN
Situation in France :
OSIRIS MTR shutdown 2015

## Slide 6
R&D in support to nuclear Industry
  Safety and Plant life time management (ageing & new plants)
  Fuel behavior validation in incidental and accidental situation
  Assess innovations and related safety for future NPPs
Radio-isotopes supply for medical application
  99Mo production
    JHR will supply 25% of the European demand (today about 8 millions protocols/year)
    + Up to 50% upon specific request
A key tool to support expertise
  Training new generations (JHR simulator, secondees program)
  Maintaining a national expertise staff and credibility for public acceptance
  Assessing safety requirements evolution and international regulation harmonization
Jules Horowitz Reactor
1. Context and objectives of the JHR
main objectives
Notes: The Main Objectives of JHR
1] Support to nuclear industry, Regulators and R&D institutes
2] MOLI Production for Medical applications
3] Support Expertise: a key objective for the European Commission explaining their involvment in the consortium to maintain Epertise in Europe

## Slide 7: 2. General figures of the JHR

## Slide 8: 2. General figures of the JHR
MTR allows to reproduce on
a small scale, real power plant
conditions and in some cases,
more severe conditions for :
  Material screening (comparison of materials tested under representative conditions)
  Material characterisation (behaviour of one material in a wide range of operating conditions, up to off-normal and severe conditions)
  Fuel element qualification (test of one or several fuel rods)
Circuits (thermohydraulic,
chemistry, purification,…)
In-pile test device
PAGE 8

## Slide 9: General layout of the JHR site
Warehouse and
cold workshop
Offices
Cooling systems
Changing rooms +
power supply
Reactor pool
(DD, NDE)
Experimental
rooms
Storage pools (NDE)
Control room
Hot cells
(NDE + handling)
Reactor Building
Laboratories
2. General figures of the JHR
PAGE 9
Nuclear Auxiliary Building

## Slide 10
FP laboratory
dedicated to on-line FP measurement
Cubicle ; Control of Thy conditions and water treatment
piping penetration
Connection lines
Reactor vessel
Test device
I&C rooms for loop + test device
Core
2. General figures of the JHR
PAGE 10
Reactor building

## Slide 11
The core is under moderated:
High fast neutron flux in the core
High thermal neutron flux in the reflector
2. General figures of the JHR
PAGE 11
In reflector
Up to 5.5 10
14
n/cm
²
.s
~20 fixed positions
(
100mm ; 1 position
200mm)
and 6 displacement systems
Fuel studies: up to
600 W/cm with a
1%
235
U PWR rod
In core
Up to 5.5 10
14
n/cm
²
.s > 1
MeV
Up to 10
15
n/cm
²
.s > 0.1
MeV
Displacement systems:
•
Adjust the fissile power
•
Study transients
Fuel experiment
(fast neutron flux
–
GEN IV)
7 Small locations (
F
~ 32 mm)
3 Large locations (
F
~
80 mm)
Material ageing
(low ageing rate)
~20 simultaneous
experiments
Core Designed for UMo
Al fuel
Start
-
up with U
3
Si
2
-
Al fuel
70 MWth / 100 MWth
25 to 30 days cycle length
6
-
7 days shutdown
1/Lethargy
Material ageing
(up to 16
dpa/y
)
GEN II & III + GEN IV

## Slide 12: 2. General figures of the JHR
In reflector (moving system)
In core and in reflector
Fast flux
Thermal flux
A large range of neutron fluxes and spectra
(and possible adaptation with « neutron filters »)
Neutron spectra
PAGE 12

## Slide 13: 3. Experimental capabilities of the JHR

## Slide 14: Hosting experimental systems (dedicated to LWR fuel testing)
PAGE 14
MADISON
For fuel testing under nominal conditions
ADELINE
For fuel testing under
off-normal conditions
Power transient,
post clad failure fuel behavior,
Lift-off experiment…
LORELEI fuel testing under accidental conditions (LOCA)
Source Term (FP releases)
Rod thermal-mechanical behaviour
Ballooning and clad burst (fuel relocation)
Corrosion at high temperature
Quenching and post-quench behaviour
3. Experimental capabilities of the JHR
Available at JHR start-up
Available at JHR start-up

## Slide 15
29 octobre 2017
PAGE 15
- Irradiated material behaviour
tensile tests, resilience test (Charpy), crack propagation tests …..
Behaviour of Thermal affected zones
CLOE Corrosion loop
for “Zr alloy Corrosion” and “Irradiation Assisted Stress Corrosion Cracking”
OCCITANE
For pressure vessel steel testing
CALIPSO, MICA
For material testing
under high dpa
and accurate temperature control
(+ mechanical loading)
Hosting experimental systems (dedicated to LWR material testing)
3. Experimental capabilities of the JHR
MICA Available at JHR start-up

## Slide 16: Non Destructive Examination (NDE) Benches
Gamma and X-Ray tomography systems
Multipurpose test benches
Coupled Gamma &X-ray bench
Coupled X-ray & g bench in storage pool
Neutron imaging system in reactor pool
Coupled X-ray & g bench in reactor pool
Test device
examination in pools
Sample examination
in hot cells
  Initial checks of the experimental loading
  Adjustment of the experimental protocol
  On-site NDE tests after the irradiation phase
Neutron Imaging System
3. Experimental capabilities of the JHR

## Slide 17: 4. JHR consortium and collaborations

## Slide 18
4. JHR consortium and collaborations
JHR Consortium : economical model for investment & operation
  CEA = Owner & nuclear operator with all liabilities
  JHR Members owner of Guaranteed Access Rights
    (in proportion of their financial commitment to the construction)
  A Member can use totally or partly his access rights for implementing proprietary programs with full property of results and/or for participating to the Joint International Programs open to non-members
  Open to new member entrance until JHR completion
JHR Consortium current partnership: Research centers & Industrial companies
IAEC
Associated Partnership: JAEA
PAGE 18

## Slide 19
  Strong CEA intention to welcome Junior and/or Senior Scientists, Nuclear Engineers, Operators, Safety Managers… within JHR teams for various topics (R&D programs, Hands-on training on equipment…)
Since CEA designation in September 2015, 6 Member States from the IAEA have signed an Agreement with CEA
  Objectives of the CEA-ICERR (IAEA Terms of Ref):
  Create international scientific networks
  Make available CEA facilities and experience to affiliates
  Lead innovative joint programs with shared results
  Enhance utilization of Research Reactors
  Host international scientists / engineers (visiting scientists, operators…)
  Provide “hands on” nuclear education “in the field”
THE JHR AND ANCILLARY FACILITIES AS AN “ICERR”
4. JHR consortium and collaborations
PAGE 19

## Slide 20: 5. Status of the reactor construction

## Slide 21
Civil work of Reactor Building and Auxiliary Unit Building nearly completed
Delivery of Hot Cells
end of 2016
(Czech partners)
Preparation for pool liner setting-up
5. Status of the reactor construction

## Slide 22
December 2016
March 2017
5. Status of the reactor construction
March 2017 : NUCLEAR UNIT CLOSURE
PAGE 22

## Slide 23
Horse saddle flange
Last welding on the vessel
Electron beam welding
Rack for fuel elements
Main water box with primary system connection
Heat Exchangers (Spanish partner)
Core components
5. Status of the reactor construction

## Slide 24
JHR Fuel qualification
(EVITA Program performed in BR2)
5. Status of the reactor construction
PAGE 24

## Slide 25: 6. The key-role of innovative instrumentation for the JHR

## Slide 26: 6. The key-role of innovative instrumentation for the JHR
Illustration of measurement needs for material testing
Objectives of irradiation tests :
Assess / verify / increase the precision of
behavior laws under irradiation
Integrated flux / dose
Studied property
(ex : fragility, cracking, corrosion, conductivity, etc.)
Influence parameter
(temperature, physicochemical conditions, etc.)
 All these parameters must be accurately measured !
Watch safety parameters
= check that some specified parameters stay in their acceptable range
(e.g. : temperature, pressure, etc.)
Monitor the experiments
damages
In-pile measurements are essential to:
PAGE 26

## Slide 27: 6. The key-role of innovative instrumentation for the JHR
Main stakes for in-pile instrumentation
Reduction of uncertainties in experimental conditions
- Neutrons / gamma flux
- Neutron spectrum
- Neutron dose
Better knowledge of nuclear heating
 design of experimental devices
Major stakes for JHR
Highly instrumented experiments
« Cook and look » 
Online measurement of experimental parameters
Material behavior
New materials, better representativeness
- Temperature
- Deformations (creep…)
Better characterization of thermo-hydraulic conditions
 temperature field / fluid flows
Fuel improvement and qualification
- Fission gas release
- Pellet-cladding interaction
- Accidental conditions (LOCA)
Radiation measurements
Physical parameter measurements
Advanced in-pile instrumentation is necessary to answer needs coming from advanced simulation then enhance the quality of the future JHR experiments
PAGE 27

## Slide 28: 6. The key-role of innovative instrumentation for the JHR
PAGE 28
In-pile test resources
BR2 and BR1 reactors (SCK•CEN Mol)
TRIGA reactor (JSI Ljubljana)
MARIA reactor (NCBJ Świerk)
ATR reactor (INL Idaho Falls)
MIT reactor (MIT Boston)…
Manufacturing resources
Fission chamber manufacturing workshop
CEA Cadarache
Development and test resources
Metrology platform
CEA Cadarache
Optics laboratory
CEA Saclay
Acoustics laboratory
IES Montpellier
Calorimetry laboratory
Aix-Marseille University
MINERVE reactor
CEA Cadarache
Signal analysis laboratory
CEA-Tech Saclay
Implementation (RJH)
CEA Cadarache
Sensor modelling platform
CEA Cadarache
MADERE dosimetry platform
CEA Cadarache
OSIRIS and ISIS reactors
CEA Saclay
Material resources and facilities

## Slide 29
ZPR Instrumentation
Low activity measurements
Nuclear heating
PAGE 29
In-pile optical measurements
Acoustic imagery
Acoustics
Radiation and heating measurements
MTR Instrumentation
(LVDT, Corrosion)
MTR Instrumentation (optics, ultrasounds, fission chambers…)
Neutron measurement and analysis
Neutron and gamma measurements
SiC sensors
Current collaborations for in-core instrumentation
JSI
calibration,
inter-comparisons,
X spectrometry
Activation dosimetry
LDCI
4. JHR consortium and collaborations

## Slide 30: 6. The key-role of innovative instrumentation for the JHR
Fast Neutron Detection System
FNDS is the first and unique acquisition system able to provide an online measurement of the fast neutron flux (E>1MeV) in typical MTR conditions
 FNDS proved its ability to measure online both thermal and fast neutron flux (consistency with activation dosimetry is better than 5%).
FNDS has been validated in 2015 after successive tests at the Belgium BR2 reactor and at the French ISIS reactor (FNDS signal was compared to reference thermal and fast neutron flux measurements using activation dosimeters)
PAGE 30

## Slide 31
Fission gas analysis : Acoustic measurements
PAGE 31
Online measurement of the molar mass of the gas inside the fuel rod ( fraction of released fission gas)
10-year development
Operated successfully on a high burn-up MOX fuel rod in the REMORA-3 experiment (OSIRIS) & Excellent accuracy of the measurement (vs post-irrad. Meas.)
PAGE 31
6. The key-role of innovative instrumentation for the JHR

## Slide 32: 6. The key-role of innovative instrumentation for the JHR
MELODIE: Mechanical Loading Device for Irradiation Experiments
  Technical goals
  Study of LWR cladding irradiation creep
  Hoop stress 120 MPa, biaxiality ratio 0 to 1
  Biaxial online control of the stress
  Biaxial online measurement of the creep
  Why
  New technology for future instrumented experiments in the JHR
  Anisotropic material calls for complex experiments
  Cladding life is multiaxial because of the combination of FGR and PCMI
  First irradiation in Osiris performed in 2015 was very promising: optimization of the device is going-on
Creep rate @ 60 Mpa ≈ 4 µm/day
Creep rate @ 110 Mpa ≈ 8 µm/day
PAGE 32

## Slide 33: Future MTR capabilities : Jules Horowitz Reactor
General conclusion
Material Testing Reactors remains key-tools in R&D support for nuclear power industry
Research Reactors are now more “costly machines” than in the past…
Considering the increasing complexity of the experiments (due to enhanced requirements from simulation) the use of international platform (as will be JHR) is recommended
Innovative in-core instrumentation is a key for the quality and attractiveness of future MTR experimental programs, together with Post-Irradiation Analysis capabilities
PAGE 33

## Slide 34: Nuclear Energy Division Reactor Studies Department Experimental Physics Section Instrumentation Sensors and Dosimetry Laboratory
French alternative energies and atomic energy commission
Cadarache | F-13108 Saint-Paul-lez-Durance | France
T. +33 (0)4 42 25 79 62 | F. +33 (0)4 42 25 78 76
Etablissement public à caractère industriel et commercial
RCS Paris B 775 685 019