Sensors, Energy harvesting, wireless Network & Smart Objects Conference 2017

Deposition of doped and undoped HfO2 for fast and low energy consumption ferroelectric devices

# J.Bouaziz1,2, B. Vilquin1, P. Rojo Romeo1, N. Baboux2 and B. Masenelli2

1Université de Lyon, Ecole Centrale de Lyon, Institut des Nanotechnologies de Lyon, CNRS UMR5270, 36 avenue Guy de Collongue, 69134 Ecully cedex, France

2Université de Lyon, INSA de Lyon, Institut des Nanotechnologies de Lyon, CNRS UMR5270, 7 avenue Capelle, 69621 Villeurbanne cedex, France

1) Context / Study motivation

IoT sensor node requires edge computing which means processing data at the source. These systems need highly energy efficient microprocessor units (MCU) using embedded non-volatile memories (eNVM). However eFLASH technology is limited by low write speed, high power and low endurance. Alternative fast, low power and high endurance eNVM could greatly enhance energy efficiency. FeRAM has the highest endurance of all emerging NVMs. However perovskite based eFeRAM is incompatible with Si CMOS, it does not easily scale and has manufacturability and cost issues.

Recently discovered doped HfO2 [1] is a promising candidate to solve these problems. HfO2 processes are already integrated in Si CMOS industry and in theory its ferroelectric properties allow us to use oxide layer thinner than 10nm. Nevertheless the endurance properties should be improved for industrial applications and the nucleation and stabilization of the ferroelectric phase (f-phase) is not well understood [2].

The f-phase in doped HfO2 is attributed to the polar orthorhombic phase (o-III phase), but other phases are present inside the oxide after the growth.

Metal/Ferroelectric/Metal(MFM) capacitor is the elementary “brick” for FeRAM in the  1Transistor-1Capacitor (1T-1C) model. Consequently the stack TiN/HfxZr1-xO2/TiN has been particularly studied as Zr-doped HfO2 exhibits quite good endurance and retention properties [3-5].

Consequently, the stack TiN/HfxZr1-xO2/TiN seems to be adapted for new fast and low energy consumption FeRAM, but more studies on the phase transition conditions are required.

2) Description of approach and techniques

In this work, we study different materials in order to build MFM capacitors. We have deposited TiN by reactive sputtering in different conditions. We have deposited (Hf,Zr)O2 solid solution, HfO2 and ZrO2 made by magnetron reactive sputtering respectively from an alloy target of Hf/Zr, from a Hf and Zr target, and also HfO2 by non-reactive sputtering from a HfO2 target as insulator oxides on Pt and TiN as electrodes. We compare (Hf,Zr)O2 solid solution behaviour with undoped HfO2 and undoped ZrO2 behaviour. X-rays Diffraction (XRD) are proceeded to characterize structural properties. I(V) and C(V) characterization are performed for Pt/(Hf,Zr)O2/Pt stacks and we measure the resistivities of all electrodes.

3) Results / Conclusions / Perspectives

In order to reduce the thermal budget we use low temperature in-situ annealing. XRD reveals a very similar monoclinic phase for (Hf,Zr)O2, HfO2 and ZrO2 on Pt and TiN at 350°C which seems not to be related to the thickness. This material could be used for other high-K applications.

We observed that the HfO2, ZrO2 and (Hf,Zr)O2 behaviours are not the same if we proceed by in-situ annealing inside the sputtering machine or if we proceed by post-annealing process. One origin of this difference can be attributed to a difference in annealing duration.

In order to stabilize the ferroelectric phase, complementary experiments are needed, particularly deposition at higher temperature.

For the electrodes, TiN was deposited on different substrates. Different crystalline orientations were observed with the same thickness depending on the used substrate.

These preliminary results could find other applications but also could lead us to find a pathway and a better understanding of the stabilization of the ferroelectric phase as we are completing the experimental phase diagram of HfxZr1-xO2.

Figure 1. X-rays diffraction patterns of HfO2, ZrO2 and (Hf,Zr)O2 solid solution at 350°C from respectively a Hf target, a Zr target and an alloy target of Hf/Zr with 56% of Hf and 44% of Zr by reactive sputtering on Pt. The three patterns show the nucleation of a monoclinic phase.

Figure 2. X-rays diffraction patterns of HfO2 grown from Hf or HfO2 targets by sputtering on Pt and annealed by different technics.

Figure 3.  X-rays diffraction pattern for the growth of TiN on Si and SiO2 in the same conditions by reactive sputtering.

Figure 4. C(V) and I(V) characteristics for a Pt/(Hf,Zr)O2/Pt sample showing no ferroelectric behavior.

REFERENCES :

[1]	T. S. Böscke et al., “Ferroelectricity in Hafnium Oxide Thin Films,” Applied Physics Letters 99, no. 10 (September 5, 2011): 102903, doi:10.1063/1.3634052.

[2] G. Karbasian et al., “Stabilization of ferroelectric phase in tungsten capped Hf0.8Zr0.2O2”, Appl. Phys. Lett. 111 (2017) 8–12. doi:10.1063/1.4993739.

[3] Zhen Fan et al., “Ferroelectric HfO 2 -Based Materials for next-Generation Ferroelectric Memories,” Journal of Advanced Dielectrics 6, no. 2 (June 2016): 1630003, doi:10.1142/S2010135X16300036.

[4] Nanbo Gong and Tso-Ping Ma, “Why Is FE–HfO 2 More Suitable Than PZT or SBT for Scaled Nonvolatile 1-T Memory Cell? A Retention Perspective,” IEEE Electron Device Letters 37, no. 9 (September 2016): 1123–26, doi:10.1109/LED.2016.2593627.

[5] Min Hyuk Park et al., “Ferroelectricity and Antiferroelectricity of Doped Thin HfO2-Based Films,” Advanced Materials, 2015, 1811–31, doi:10.1002/adma.201404531.