SUPPORTING INFORMATION

New lanthanide-based coordination polymers with 2,5-dihydroxyterephthalate.

Jinzeng Wang, Carole Daiguebonne, Yan Suffren, Stéphane Freslon, Guillaume Calvez, Kevin Bernot and Olivier Guillou*

Univ Rennes, INSA Rennes, CNRS UMR 6226 "Institut des Sciences Chimiques de Rennes", F-35708 Rennes

*To whom correspondence should be addressed.

Figure S1. Experimental X-ray diffraction diagram of Na2(H2-dhbdc)·0.5H2O

Crystal structure of [Na(H3-dhbdc)(H2O)2]∞

[Na(H3-dhbdc)(H2O)2]∞ crystallizes in the monoclinic system, space group P21/n (n°14) with the following cell parameters: a = 8.8788(6) Å, b = 6.8920(5) Å, c = 16.2174(12) Å, β = 96.259(3)°, V = 986.47(12) Å3 and Z = 4. There are one sodium ion, one once deprotonated ligand (H3-dhbdc-) and two water molecules bound to the sodium ion in the asymmetric unit (Figure S1).

Figure S2. Asymmetric unit with atom labels (left), sodium ion neighborhood (top right) and µ4-H3-dhbdc- ligand (bottom right) in [Na(H3-dhbdc)(H2O)2]∞.

The sodium ion is six-coordinated by two oxygen atoms from two water molecules (O8 and O7) and four oxygen atoms from four different µ4-H3-dhbdc- ligands that form a slightly distorted octahedron. The once deprotonated ligand connects four sodium ions: One is bound to the deprotonated carboxylate in an unidentate way, two others are bounded in an unidentate way to the two oxygen atoms of the carboxylic acid function and the third one is bound in an unidentate way as well to one of the hydroxyl group. The crystal structure is 3D as shown in Figure S2. Selected crystal and final structure refinement data are gathered in Table S1

Figure S3. Projection views of [Na(H3-dhbdc)(H2O)2]∞.

| Table S1. Crystallographic data for [Na(H3-dhbdc)(H2O)2]∞. |  |
| --- | --- |
| Chemical formula | C8H9NaO8 |
| System | monoclinic |
| Space group (n°) | P21/n (n°14) |
| Formula weight (g.mol-1) | 256.14 |
| a (Å) | 8.8788(6) |
| b (Å) | 6.8920(5) |
| c (Å) | 16.2174(12) |
|  | 96.259(3) |
| V (Å3) | 986.47(12) |
| Z | 4 |
| θ range (°) | 2.507-27.516 |
| Dcalc (g.cm-3) | 1.725 |
| R | 0.0404 |
| Rw | 0.1237 |
| GoF | 1.137 |
| min/max (e.Å-3) | -0.38/0.40 |
| CCDC number | 1913157 |

Figure S4. Experimental powder X-ray diffraction diagrams of [Ln2(H2-dhbdc)3(H2O)126H2O] (Ln = La-Nd) and simulated powder X-ray diffraction diagram of [La2(H2-dhbdc)3(H2O)126H2O] on the basis of its crystal structure.

Figure S5. Experimental powder X-ray diffraction diagrams of [Ln2(H2-dhbdc)3(H2O)86H2O] (Ln = Sm-Lu plus Y) and simulated powder X-ray diffraction diagram of [Er2(H2-dhbdc)3(H2O)86H2O] on the basis of its crystal structure.

| Table S2 Elemental analyses of the micro-crystalline powders of the lanthanide-based coordination polymers |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Ln | MW (g.mol-1) | % Ln found(calc.) | % C found(calc.) | % H found(calc.) | % O found(calc.) |
| La | 1190 | 23.1(23.4) | 24.3(24.2) | 4.1(4.0) | 48.5(48.4) |
| Ce | 1192 | 24.0(23.5) | 24.0(24.2) | 4.0(4.0) | 48.0(48.3) |
| Pr | 1194 | 23.5(23.6) | 24.0(24.1) | 3.9(4.0) | 48.6(48.2) |
| Nd | 1200 | 24.5(24.0) | 24.2(24.0) | 3.8(4.0) | 47.5(48.0) |
| Sm | 1141 | 26.3(26.4) | 25.0(25.2) | 3.7(3.5) | 45.0(44.9) |
| Eu | 1144 | 27.0(26.6) | 25.0(25.2) | 4.0(3.5) | 44.0(44.8) |
| Gd | 1155 | 27.5(27.3) | 25.0(24.9) | 3.3(3.5) | 44.2(44.3) |
| Tb | 1158 | 27.5(27.5) | 24.5(24.9) | 3.5(3.5) | 44.5(44.2) |
| Dy | 1165 | 28.0(27.9) | 25.0(24.7) | 3.0(3.4) | 44.0(43.9) |
| Ho | 1170 | 28.5(28.2) | 24.5(24.6) | 3.5(3.4) | 43.5(43.8) |
| Er | 1175 | 28.5(28.5) | 24.7(24.5) | 3.5(3.4) | 43.3(43.6) |
| Tm | 1178 | 29.0(28.7) | 24.0(24.4) | 3.5(3.4) | 43.5(43.5) |
| Yb | 1186 | 29.0(29.2) | 24.0(24.3) | 3.0(3.4) | 44.0(43.2) |
| Lu | 1190 | 29.8(29.4) | 24.5(24.2) | 4.0(3.4) | 41.7(43.0) |
| Y | 1018 | 17.1(17.5) | 28.6(28.3) | 4.0(3.9) | 50.3(50.3) |

Figure S6. Thermal analyses of [La2(H2-dhbdc)3(H2O)126H2O].

Figure S7. Thermal analyses of [Er2(H2-dhbdc)3(H2O)86H2O].

Figure S8. Solid-state emission spectra of [La2(H2-dhbdc)3(H2O)126H2O] at variable temperature (top). Integrated area vs temperature with curve fit (linear fitting) of [La2(H2-dhbdc)3(H2O)126H2O] between 77 and 293 K (middle). Energy band maxima (Emax in nm), band widths at half height (FWHM in nm) with their trends of [La2(H2-dhbdc)3(H2O)126H2O] between 77 and 293 K (bottom).

[La2(H2-dhbdc)3(H2O)126H2O] compound shows a relatively strong phosphorescence at room temperature that increases by 150% at 77 K. We also observe a significant decrease by around 25% of the widths (FWHM) of the emission band at low temperature with a reduction of the vibronic effects (-0.2 nm/K). The energy band maxima of the emission band changes slightly between 293 and 77 K, we observe a small shift towards the lower wavelengths by decreasing the temperature until 140 K then a small shift towards the longer wavelengths between 140 and 77 K.

Figure S9. Room temperature solid-state absorption spectrum of [Gd2(H2-dhbdc)3(H2O)8∙6H2O]∞.