SUPPORTING INFORMATION.

Non-covalent interactions in hexanuclear polyoxidometalates [VIV6B20O50H8]8-. An experimental and theoretical approach.

Karina Muñoz-Becerra1¥, Kerry Wrighton-Araneda1†, Eric Le Fur2, Jean-Yves Saillard3, Samia Kahlal3, Olivier Cador3, Verónica Paredes-García4,5, Diego Venegas-Yazigi*1,4

1Facultad de Química y Biología, Universidad de Santiago de Chile, USACH, Av. Libertador Bernardo O’Higgins 3363, Estación Central, Región Metropolitana, Santiago, Chile.

2Department Univ Rennes, ENSCR, CNRS ISCR-UMR 6226 F-35000 Rennes, France

3Department Univ Rennes, CNRS ISCR-UMR 6226 F-35000 Rennes, France

4Centro para el Desarrollo de la Nanociencia y Nanotecnología, CEDENNA, Santiago, Chile

5Departamento de Ciencias Químicas, Universidad Andrés Bello, Santiago, Chile.

¥Present address: Dirección de Investigación y Postgrado, Universidad de Aconcagua, Pedro de Villagra 2265, Vitacura, Chile.

†Present address: Programa Institucional de Fomento a la Investigación, Desarrollo e Innovación. Universidad Tecnológica Metropolitana. Ignacio Valdivieso 2409, P.O. Box 8940577, San Joaquín, Santiago, Chile.

Content

- Elemental analysis for compounds 1 – 3.

- Calculated and measured PXRD patterns of compounds 1 – 3.

- FT-IR spectra and the corresponding assignments for compounds 1 – 3.

- Figure S1. Crystalline packing of compound 1.

- Figure S2. Crystalline packing of compound 2.

- Figure S3. Crystalline packing of compound 3.

- Figure S4. Representation of the dinuclear K–(O2)–K unit.

- Figure S5. NCIPlot analysis surfaces for V6-polyanions with comments.

- Figure S6. Experimental and fitted temperature dependence of cMT for (a) 1, (b) 2, and (c) 3.

- Table S1. Crystal data and structure refinement for compounds 1 – 3.

- Table S2. Selected bond distances and selected angles for compounds 1 – 3.

- Table S3. Distances and angles measurements for V6-rings of compounds 1 – 3.

- Table S4. Selected interatomic parameters for the V6- rings of compounds 1 – 3.

- Table S5. K – O distances for compounds 2 and 3.

- Table S6. Magnetic parameter fitted of compounds 1 − 3.

- Table S7. Calculated SHAPE† values for compounds 1, 2, and 3.

- Table S8. Experimental absorption energy values of the UV-visible spectra for compounds 1 – 3.

- Elemental analysis.

|  | Calculated |  |  | Experimental |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Compound | %C | %N | %H | %C | %N | %H |
| 1 | 8.45 | 6.57 | 3.79 | 8.00 | 6.89 | 3.74 |
| 2 | 5.18 | 6.04 | 2.61 | 5.03 | 5.83 | 2.81 |
| 3 | 4.14 | 3.22 | 3.13 | 6.95 | 4.58 | 3.06 |

- Comparison of PXRD patterns measured (up) and calculated spectra (down) from single crystal data for compounds 1 – 3.

3. Assignation of the FT-IR spectra for 1 – 3.

(NH3CH2CH2CH2NH3)4{V6B20O50H8}·4H2O 1. The bands of the FT-IR spectrum were assigned as follows: ν (V – O – V) (bands at 766 cm-1 and 820 cm-1), ν(V = O) (928 cm-1), ν (B – O) (three bands 1022-1158 cm-1) of (BO4), and ν (B – O) (two bands 1366-1402 cm-1) of (BO3), δ(N-H) and δ(O-H) (1639 cm-1), ν(N –H) and ν(O –H) (strong bands between 3078 – 3412 cm-1).

K2(NH3CH2CH2NH3)2.5(NH3CH2CH2NH2){V6B20O50H8}·2H2O 2. The bands of the FT-IR spectrum were assigned as follows: ν (V – O – V) (bands at 764 cm-1 and 822 cm-1), ν(V = O) (two bands of 905 and 926 cm-1), ν (B – O) (three bands 1027-1158 cm-1) of (BO4), and ν (B – O) (1401 cm-1) of (BO3), δ(O-H) (1630 cm-1), ν(N –H) and ν(O –H) (strong bands between 3241 – 3381 cm-1).

K2(NH3CH2CH2CH2NH3)2(H3O)2{V6B20O50H8}·8H2O 3. The bands of the FT-IR spectrum were assigned: ν (V – O – V) (bands at 762 cm-1 and 818 cm-1), ν(V = O) (920 cm-1), ν (B – O) (three bands 1027-1163 cm-1) of (BO4), and ν (B – O) (1400 cm-1) of (BO3), δ(N-H) and δ(O-H) (1631 cm-1), ν(N –H) and ν(O –H) (strong bands at 3223 – 3344 cm-1).

Figure S1. Crystalline packing of (NH3CH2CH2CH2NH3)4{V6B20O50H8}·4H2O 1 along the ac plane. Vanadium atoms are shown in polyhedral representation. In the inset is shown the inter-cluster connectivity described in the main manuscript for 1.

Figure S2. Crystalline packing of K2(NH3CH2CH2NH3)2.5(NH3CH2CH2NH2){V6B20O50H8}·2H2O 2 along the ac plane. K–O interactions are shown as red dots. Vanadium atoms are depicted in polyhedral representation. The intercluster space is occupied by K cations, mono- and diprotonated ethylenediamine molecules (omitted for clarity), along with water crystallization molecules.

Figure S3. Crystalline packing of K2(NH3CH2CH2CH2NH3)2(H3O)2{V6B20O50H8}·8H2O 3 along the ac plane. K – O interactions are shown as red dots. Vanadium atoms are shown in polyhedral representation.

Figure S4. The dinuclear K–(O2)–K unit connecting four polyanions. Each K atom is octa-coordinated. The coordination environment of each K atom is shown as a polyhedral representation. The graphical representation is given with four [V6B20O50H8]8- polyanions. The atoms labels are referred to compound 3.

Figure S5. NCI 3D representation iso-surfaces for three representative cases: (a) naked [V6B20O50H8]8-, (b) [V6B20O50H8]8- surrounded by a 1,3-diapH+ amine cation, and (c) [V6B20O50H8]8- surrounded by a K cation (both cations are positioned into their original crystallographic positions), and  NCIPlot s(λ) graphs for (d) [V6B20O50H8]8-, (e) [V6B20O50H8]8-···1,3-diapH+, and (f) [V6B20O50H8]8-···K.

The NCIPlot analysis was carried out considering the different crystalline packing of the V6-systems. This analysis allows to differentiate the contribution of non-covalent attractive, repulsive, and weak interactions (vdW), associated as signals or singularities observed in the s(λ) graph at low-density (λ) and low-reduced gradient (s), in accordance with the scale shown in the top of the figure (λ < 0, λ  ̴ 0 and λ > 0, respectively). In Figure S5 is observed that for the naked [V6B20O50H8]8- cluster (a) the electrostatic interactions are mainly of the steric type (red surfaces in (a), and a considerable contribution of signals at low-density >0, and low-reduced gradient in (d)), with a poor contribution of van der Waals or attractive interactions within it (since a poor presence of signals or singularities at low-density and low-reduced gradient with λ < 0 and λ  ̴ 0 was observed in (d)). The high repulsive surfaces located into the V6-cluster are attributed to their high overall charge and to the excess of electrons.

When a 1,3-diapH+ amine cation was introduced in the analysis, weak van der Waals interactions appear, while both repulsive and hydrogen bonds interactions increase (considerable signals contributions at low-density and low-reduced gradient at λ < 0, λ  ̴ 0 and λ > 0 in (e)). The attractive forces (green and light-blue surfaces in (b)) are given by the H···O non-covalent interactions, with the most stabilizing force the interaction between the protonated amine group with the oxygen atom of the terminal [BO3] groups (b,e).

Finally, when a K cation was considered in the analysis, a more defined contribution signals to the van der Waals interactions were observed (signals at low-density and low-reduced gradient at λ  ̴ 0 in (f)) in comparison with the naked cluster and with that interacting with a 1,3-diapH+ cations. In this case, the K···O interaction shows little surfaces compared with the previous case (green surface in (c)). Nevertheless, in this case the K···O interaction occurs by a permanent Coulombic interaction from point charge as is expected for the electrostatic potentials and are mainly directed to the {V6IVO18}12- central ring. With this simple analysis it is demonstrated that K cations have a major incidence over the net electrostatic interactions present in the crystalline systems that can be associated with their important influence to modulates the magnetic coupling of the V6-rings.

Figure S6. Experimental and fitted temperature dependence of cMT for (a) 1, (b) 2, and (c) 3.

Table S1. Crystal data and structure refinement for compounds 1 – 3.

|  | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Formula | C12H64B20N8O54V6 | C7H42B20K2N7O50V6 | C6H54B20K2N4O60V6 |
| Moiety formula | (NH3CH2CH2CH2NH3)4[V6B20O50H8] · 4H2O | K2(NH3CH2CH2NH3)2.5(NH3CH2CH2NH3)[V6B20O50H6]· 2H2O | K2(NH3CH2CH2CH2NH3)2 (H3O)2 [V6B20O50H6]·8H2O |
| Formula weight | 1706.04 | 1624. 40 | 1742.14 |
| T/K | 293(2) | 293(2) | 293(2) |
| Crystal system | Monoclinic | Triclinic | Triclinic |
| Space group | P 21/n | P -1 | P -1 |
| a/Å | 14.297(3) | 11.0439(8) | 11.051(5) |
| b/Å | 13.282(3) | 12.0556(8) | 12.078(5) |
| c/Å | 15.738(3) | 12.3168(8) | 12.242(5) |
| α (°) | 90.000 | 93.364(1) | 92.592(5) |
| β (°) | 96.43(3) | 112.256(1) | 111.884(5 |
| γ (°) | 90.000 | 111.285(1) | 111.389(5) |
| V/Å3 | 2969.7(10) | 1377.10(16) | 1380.4(10) |
| Z | 2 | 1 | 2 |
| Density (calculated) (g cm-3) | 1.895 | 1.962 | 4.191 |
| Absorption coefficient (mm-1) | 1.038 | 1.271 | 2.545 |
| F(0 0 0) | 1700.0 | 793.6 | 849.0 |
| Cristal size (mm3) | 0.41 x 0.38 x 0.15 | 0.36 x 0.32 x 0.11 | 0.39 x 0.33 x 0.13 |
| ϴ range for data collection (°) | 3.02 to 27.49 | 1.83 to 26 | 3.39 to 20 |
| Index ranges | -18 ≤ h ≤ 18 -17 ≤ k ≤ 17 -20 ≤ l ≤ 20 | -13 ≤ h ≤ 13 -14 ≤ k ≤ 14 -15 ≤ l ≤ 15 | -13 ≤ h ≤ 13 -14 ≤ k ≤ 14 -15 ≤ l ≤ 13 |
| Reflection collected | 35077 | 10748 | 15901 |
| Independent reflections | 6818[R(int) = 0.0746] | 5410[R(int) = 0.0120] | 5422[R(int) = 0.0237] |
| Refinement method | Full-matrix least-squares on F2 | Full-matrix least-squares on F2 | Full-matrix least-squares on F2 |
| Goodness-of-fit on F2 | 1.060 | 1.112 | 1.077 |
| Final R indices [I >= 2σ (I)] | R1 = 0.0518 wR2 = 0.1162 | R1 = 0.0441 wR2 = 0.1219 | R1 = 0.0500 wR2 = 0.1365 |
| R indices (all data) R1 / wR2 | R1 = 0.0896 wR2 = 0.1374 | R1 = 0.0491 wR2 = 0.1246 | R1 = 0.0592 wR2 = 0.1452 |
| Largest diff. peak and hole e. Å-3 | 1.26 and -0.80 | 1.93 and -1.19 | 1.52 and -1.15 |
| CCDC number | 984059 | 984061 | 984062 |

Table S2. Selected bond distances and selected angles for compounds 1 - 3.

| 1 |  | 2 |  | 3 |  |
| --- | --- | --- | --- | --- | --- |
| Bond | Length (Å) | Bond | Length (Å) | Bond | Length (Å) |
| V1 = O1 | 1.628(3) | V1 = O17 | 1.608(2) | V1 = O3 | 1.607 (3) |
| V1 – O4 | 1.955(3) | V1 – O21 | 1.949(2) | V1 – O1 | 1.960 (3) |
| V1 – O9 | 1.959(3) | V1 – O23 | 1.958(2) | V1 – O2 | 1.966(3) |
| V1 – O5 | 1.943(3) | V1 – O14 | 1.964(2) | V1 – O12 | 1.951(3) |
| V1 – O8 | 1.958(3) | V1 – O16 | 1.966(2) | V1 – O7 | 1.959(3) |
| V2 = O2 | 1.619(3) | V2 = O20 | 1.613(2) | V2 = O6 | 1.612(3) |
| V2 – O5 | 1.954(3) | V2 – O21 | 1.949(2) | V2 – O4 | 1.958 (3) |
| V2 – O8 | 1.965(3) | V2 – O15 | 1.950(2) | V2 – O23 | 1.971 (3) |
| V2 – O6 | 1.948(3) | V2 – O14 | 1.970(2) | V2 – O1 | 1.943(3) |
| V2 – O7 | 1.956(3) | V2 – O22 | 1.975(2) | V2 – O2 | 1.960 (3) |
| V3 = O3 | 1.622(3) | V3 = O12 | 1.614(2) | V3 = O5 | 1.610(3) |
| V3 – O6 | 1.951(3) | V3 – O16 | 1.938(2) | V3 – O7 | 1.970(3) |
| V3 – O7 | 1.963(3) | V3 – O15 | 1.9540(19) | V3 – O12 | 1.948 (3) |
| V3 – O9 | 1.959(3) | V3 – O23 | 1.956(2) | V3 – O4 | 1.960 (3) |
| V3 – O4 | 1.963(3) | V3 – O22 | 1.974(2) | V3 – O23 | 1.968(3) |
| V1···V2 | 3.0400(10) | V1···V2 | 3.0543(7) | V1···V2 | 3.0375(14) |
| V2···V3 | 3.0466(11) | V2···V3 | 3.0538(6) | V2···V3 | 3.0560 (15) |
| V3···V1’ | 3.0533(10) | V3···V1’ | 3.0341(6) | V3···V1’ | 3.0541(14) |
| Angle | ° | Angle | ° | Angle | ° |
| O5 - V1 = O1 | 109.40(14) | O17 = V1 - O21 | 111.66(11) | O1 - V1 = O3 | 110.28(15) |
| O4 - V1 = O1 | 109.07(13) | O17 = V1 - O23 | 107.09(11) | O2 - V1 = O3 | 107.51(14) |
| O9 - V1 = O1 | 110.17(14) | O21 - V1 - O23 | 141.25(8) | O7 - V1 = O3 | 108.45(15) |
| O8 - V1 = O1 | 109.13(14) | O17 = V1 - O14 | 108.60(10) | O12 - V1 = O3 | 110.83(15) |
| O8 - V1 – O4 | 141.79(12) | O21 - V1 - O14 | 77.10(8) | O1 - V1 – O7 | 141.27(12) |
| O5 - V1 – O9 | 140.42(12) | O23 - V1 - O14 | 91.18(8) | O2 - V1 – O12 | 141.66(12) |
| O4 - V1 – O5 | 89.28(12) | O17 = V1 - O16 | 109.77(10) | O1 - V1 – O12 | 89.42(12) |
| O5 - V1 – O8 | 77.74(11) | O21 - V1 - O16 | 89.24(8) | O1 - V1 – O2 | 77.40(11) |
| O4 - V1 – O9 | 77.11(11) | O23 - V1 - O16 | 77.30(8) | O2 - V1 – O7 | 90.95(12) |
| O8 - V1 – O9 | 90.28(11) | O14 - V1 - O16 | 141.63(8) | O7 - V1 – O12 | 77.08(12) |
| O5 – V2 = O2 | 108.58(15) | O20 = V2 - O21 | 110.35(11) | O1 – V2 = O6 | 107.03(14) |
| O6 – V2 = O2 | 110.03(15) | O20 = V2 - O15 | 110.84(11) | O2 – V2 = O6 | 106.47(14) |
| O7 – V2 = O2 | 110.85(15) | O21 - V2 - O15 | 138.81(8) | O4 – V2 = O6 | 110.69(14) |
| O8 – V2 = O2 | 109.68(15) | O20 = V2 - O14 | 109.31(11) | O23 – V2 = O6 | 110.15(14) |
| O5 – V2 – O6 | 89.12(12) | O21 - V2 - O14 | 76.96(8) | O2 – V2 – O4 | 142.81(12) |
| O5 – V2 – O7 | 140.58(12) | O15 - V2 - O14 | 89.55(8) | O1 – V2 – O23 | 142.82(12) |
| O6 – V2 – O8 | 140.27(12) | O20 = V2 - O22 | 107.94(11) | O1 – V2 – O4 | 89.95(12) |
| O6 – V2 – O7 | 77.35(12) | O21 - V2 - O22 | 90.39(9) | O1 – V2 – O2 | 77.94(11) |
| O7 – V2 – O8 | 89.76 | O15 - V2 - O22 | 77.15(8) | O2 – V2 – O23 | 91.54(12) |
| O5 – V2 – O8 | 77.30(11) | O14 - V2 - O22 | 142.75(8) | O4 – V2 – O23 | 77.10(11) |
| O4 – V3 = O3 | 109.56(14) | O12 = V3 - O16 | 106.73(10) | O4 – V3 = O5 | 110.55(15) |
| O6 – V3 = O3 | 110.13(14) | O12 = V3 - O15 | 110.97(10) | O7 – V3 = O5 | 109.22(15) |
| O7 – V3 = O3 | 110.34(14) | O16 - V3 - O15 | 90.05(8) | O12 – V3 = O5 | 110.40(15) |
| O9 – V3 = O3 | 107.96(14) | O12 = V3 - O23 | 106.81(10) | O23 – V3 = O5 | 108.72(15) |
| O4 – V3 – O6 | 140.27(12) | O16 - V3 - O23 | 77.99(8) | O4 – V3 – O12 | 139.05(12) |
| O7 – V3 – O9 | 141.69(12) | O15 - V3 - O23 | 142.20(8) | O7 – V3 – O23 | 142.06(12) |
| O6 – V3 – O9 | 89.35(12) | O12 = V3 - O22 | 110.11(10) | O4 – V3 – O23 | 77.12(11) |
| O6 – V3 – O7 | 77.11(12) | O16 - V3 - O22 | 143.16(8) | O4 – V3 – O7 | 89.44(12) |
| O4 – V3 – O9 | 76.92(11) | O15 - V3 - O22 | 77.06(8) | O7 – V3 – O12 | 76.91(12) |
| O4 – V3 – O7 | 90.86(12) | O23 - V3 - O22 | 91.25(9) | O12 – V3 – O23 | 90.25(12) |
| Bond | Length (Å) | Bond | Length (Å) | Bond | Length (Å) |
| B1-O7 | 1.457(5) | B1-O1 | 1.494(4) | B1-O2 | 1.465(4) |
| B1-O10 | 1.435(5) | B1-O7 | 1.483(4) | B1-O8 | 1.430(6) |
| B1-O11 | 1.541(5) | B1-O4 | 1.480(4) | B1-O9 | 1.473(7) |
| B1-O12 | 1.472(5) | B1-O18 | 1.437(4) | B1-O10 | 1.525(6) |
| B2-O8 | 1.567(5) | B2-O1 | 1.532(3) | B2-O9 | 1.366(6) |
| B2-O10 | 1.438(5) | B2-O3 | 1.432(4) | B2-O24 | 1.380(7) |
| B2-O21 | 1.526(5) | B2-O5 | 1.461(3) | B2-O25 | 1.364(7) |
| B2-O23 | 1.467(5) | B2-O15 | 1.466(4) |  |  |
|  |  |  |  | B3-O10 | 1.537(6) |
| B3-O9 | 1.474(5) | B3-O1 | 1.523(4) | B3-O11 | 1.431(6) |
| B3-O20 | 1.425(5) | B3-O6 | 1.435(4) | B3-O23 | 1.473(4) |
| B3-O21 | 1.526(5) | B3-O10 | 1.466(4) | B3-O25 | 1.460(7) |
| B3-O22 | 1.479(5) | B3-O14 | 1.474(4) |  |  |
|  |  |  |  | B4-O11 | 1.432(7) |
| B4-O12 | 1.366(5) | B4-O2 | 1.470(4) | B4-O12 | 1.468(4) |
| B4-O13 | 1.372(6) | B4-O4 | 1.533(3) | B4-O13 | 1.465(6) |
| B4-O14 | 1.364(6) | B4-O9 | 1.427(4) | B4-O14 | 1.531(6) |
|  |  | B4-O21 | 1.458(4) |  |  |
| B5-O11 | 1.539(5) |  |  | B5-O10 | 1.495(6) |
| B5-O4 | 1.461(5) | B5-O6 | 1.440(4) | B5-O14 | 1.488(5) |
| B5-O14 | 1.490(5) | B5-O7 | 1.527(4) | B5-O15 | 1.437(5) |
| B5-O15 | 1.429(5) | B5-O8 | 1.470(4) | B5-O16 | 1.495(6) |
|  |  | B5-O23 | 1.459(4) |  |  |
| B6-O5 | 1.460(5) |  |  | B6-O1 | 1.465(5) |
| B6-O15 | 1.432(5) | B6-O3 | 1.432(4) | B6-O14 | 1.526(7) |
| B6-O16 | 1.538(5) | B6-O4 | 1.532(4) | B6-O20 | 1.438(5) |
| B6-O17 | 1.482(5) | B6-O11 | 1.455(4) | B6-O21 | 1.453(6) |
|  |  | B6-O16 | 1.463(4) |  |  |
| B7-O17 | 1.375(5) |  |  | B7-O13 | 1.373(7) |
| B7-O18 | 1.374(5) | B7-O7 | 1.539(4) | B7-O21 | 1.359(7) |
| B7-O19 | 1.354(5) | B7-O9 | 1.430(4) | B7-O22 | 1.374(7) |
|  |  | B7-O13 | 1.463(4) |  |  |
| B8-O6 | 1.464(5) | B7-O22 | 1.471(4) | B8-O4 | 1.458(4) |
| B8-O16 | 1.539(5) |  |  | B8-O16 | 1.536(7) |
| B8-O19 | 1.471(5) | B8-O5 | 1.366(4) | B8-O19 | 1.467(5) |
| B8-O20 | 1.434(5) | B8-O10 | 1.365(4) | B8-O20 | 1.429(6) |
|  |  | B8-O25 | 1.374(4) |  |  |
| B9-O22 | 1.371(6) |  |  | B9-O7 | 1.469(4) |
| B9-O23 | 1.363(6) | B9-O8 | 1.368(4) | B9-O8 | 1.429(7) |
| B9-O24 | 1.380(5) | B9-O13 | 1.354(4) | B9-O16 | 1.519(6) |
|  |  | B9-O24 | 1.381(4) | B9-O17 | 1.477(5) |
| B10-O11 | 1.490(5) |  |  |  |  |
| B10-O16 | 1.485(5) | B10-O2 | 1.366(7) | B10-O17 | 1.369(7) |
| B10-O21 | 1.492(5) | B10-O11 | 1.354(9) | B10-O18 | 1.372(6) |
| B10-O25 | 1.431(5) | B10-O19 | 1.382(9) | B10-O19 | 1.369(7) |

Table S3. Selected distances and angles for the different V6-rings constituent elements for compounds 1, 2, and 3. The constituent elements are vanadium(IV) centres, oxygen atoms of the vanadyl groups (VO2+); the best medium plane between the vanadium(IV) centres; the best medium plane between the oxygen atoms of the VO2+ groups; and the horizontal plane of each vanadium(IV) SP polyhedron.

|  | Compound 1 | Compound 2 | Compound 3 |
| --- | --- | --- | --- |
| Distance between each V centre and the best medium plane on V centres | 0.005 Å | 0.006 Å | 0.003 Å |
| Angle between two planes (best medium plane on V centres and best medium plane on oxygen atoms of VO2+) | 0.66° | 0.05° | 0.17° |
| Angles between V centres |  |  |  |
| Angle (V2 -V1 - V3) | 119.87° | 118.75° | 120.65° |
| Angle (V1 -V3 - V2') | 120.07° | 120.66° | 118.64° |
| Angle (V3 -V2 - V1') | 120.05° | 120.58° | 120.70° |
| Angles between SP horizontal planes |  |  |  |
| Plane V2 - Plane V1 | 59.47° | 59.39° | 59.40° |
| Plane V1 - Plane V3 | 60.82° | 61.36° | 59.22° |
| Plane V2 - Plane V3' | 59.71° | 59.24° | 61.38° |
| Plane V3' - Plane V1' | 60.82° | 61.36° | 59.22° |
| Plane V1' - Plane V2' | 59.74° | 59.39° | 59.40° |
| Plane V2' - Plane V3 | 59.45° | 59.24° | 61.38° |

Table S4. Selected interatomic distances for the V6-rings of compounds 1 – 3.

|  | 1 | 2 | 3 |
| --- | --- | --- | --- |
| V – Ot(i) /Å | 1.607(4)-1.627(4) | 1.608(2)-1.614(2) | 1.607(3)-1.612(3) |
| V – Ob(ii) /Å | 1.938(4)-1.972(4) | 1.938(2)-1.975(2) | 1.943(3)-1.971(3) |
| V···V /Å | 3.025(1)-3.051(1) | 3.034(1)-3.054(1) | 3.037(1)-3.056(1) |
| [BO3] B-O /Å | 1.349(8)-1.381(8) | 1.353(4)-1.381(4) | 1.359(7)-1.380(7) |
| [BO4] B-O /Å | 1.432(8)-1.538(8) | 1.427(4)-1.539(4) | 1.429(7)-1.537(6) |
| V1 ··· V1’ /Å | 6.100(1) | 6.145(2) | 6.154(2) |
| V2 ··· V2’ /Å | 6.094(1) | 6.070(2) | 6.071(2) |
| V3 ··· V3’ /Å | 6.086(1) | 6.067(2) | 6.068(2) |
| CCD(iii) /Å | 12.022(3) | 11.044(5) | 11.051(5) |

Table S5. Selected K – O distances for compounds 2 and 3. The superscript indicates the number of the cluster to which the O atoms belong.

| K – O | 2 | K – O | 3 |
| --- | --- | --- | --- |
| K1–O3I / Å | 2.784(2) | K1–O6I / Å | 3.027(3) |
| K1–O11I / Å | 2.952(2) | K1–O21I / Å | 2.950(4) |
| K1–O12I / Å | 2.998(3) | K1–O20I / Å | 2.796(4) |
| K1–O12II / Å | 3.078(2) | K1–O6II / Å | 3.016(4) |
| K1–O23II / Å | 2.882(2) | K1–O2II / Å | 2.852(4) |
| K1–O17II / Å | 2.979(3) | K1–O9II / Å | 3.133(3) |
| K1–O8II / Å | 3.153(3) | K1–O3II / Å | 3.038(4) |
| K1–O25III / Å | 2.934(2) | K1–O18III / Å | 2.867(4) |

Table S6. Magnetic parameter fitted of compounds 1 − 3. J coupling constant values are in cm-1.

| Parameter | 1 | 2* | 3 |
| --- | --- | --- | --- |
| J1 | -17.6 | -11.2 | -9.2 |
| J2 | -5.5 | -3.9 | -3.2 |
| J3 | -0.4 | +2.0 | +0.5 |
| gexp | 1.91 | 1.93 | 1.93 |
| residual | 0.04329 | 0.0066 | 0.0098 |
| *IMP of 0.010 |  |  |  |

| Compound 1 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1a | 2 b | 3 c | 4 d | 5 e |
|  | PP-5 | vOC-5 | TBPY-5 | SPY-5 | JTBPY-5 |
| VANADATE 1 | 31.462 | 2.561 | 5.658 | 0.492 | 8.213 |
| VANADATE 2 | 31.312 | 2.627 | 5.845 | 0.499 | 8.473 |
| VANADATE 3 | 31.332 | 2.596 | 5.699 | 0.543 | 8.237 |
| Compound 2 |  |  |  |  |  |
|  | 1a | 2 b | 3 c | 4 d | 5 e |
|  | PP-5 | vOC-5 | TBPY-5 | SPY-5 | JTBPY-5 |
| VANADATE 1 | 30.938 | 2.63 | 5.284 | 0.571 | 7.659 |
| VANADATE 2 | 30.241 | 2.518 | 5.944 | 0.563 | 8.365 |
| VANADATE 3 | 30.928 | 2.375 | 5.84 | 0.565 | 8.273 |
| Compound 3 |  |  |  |  |  |
|  | 1a | 2 b | 3 c | 4 d | 5 e |
|  | PP-5 | vOC-5 | TBPY-5 | SPY-5 | JTBPY-5 |
| VANADATE 1 | 30.338 | 2.499 | 5.904 | 0.555 | 8.414 |
| VANADATE 2 | 30.819 | 2.354 | 6.002 | 0.571 | 8.431 |
| VANADATE 3 | 31.142 | 2.628 | 5.436 | 0.560 | 7.869 |

Table S7. Calculated SHAPE† values for compounds 1, 2, and 3.

† SHAPE. Program for the Stereochemical Analysis of Molecular Fragments by Means of Continuous Shape Measures and Associated Tools. Developed by M. Llunell, D. Casanova, J. Cirera, P. Alemany, S. Alvarez. Departament de Química Física, Departament de Química Inorgànica, and Institut de Química Teòrica i Computacional - Universitat de Barcelona.

a  1, PP-5 = pentagon (D5h)); b 2, vOC-5 = vacant octahedron (C4v); c 3, TBPY-5 = trigonal bipyramid (D3h);    d 4, SPY-5 = spherical square pyramid (C4v); e 5, JTBPY-5 = Johnson trigonal bipyramid J12 (D3h).

| Absorption band (nm) | 1 | 2 | 3 |
| --- | --- | --- | --- |
| I | 705 | 692 | 693 |
| II | 519 | 528 | 528 |
| III | 425 | 418 | 419 |
| IV | 313 | 305 | 303 |

Table S8. Experimental absorption energy values of the UV-visible spectra for compounds 1 – 3.