## Slide 1
Electronic, magnetic and structural properties of epitaxial Co2MnZ Heusler compounds
64th Annual Conference on Magnetism and Magnetic Materials
C. Guillemard, S. Petit-watelot, F. Bertran, A. M. Bataille, J.-C. Rojas-Sanchez, J. Ghanbaja, S. Andrieu

## Slide 2
Heusler compounds
Half-Metal Magnets (HMM)
Cu2MnSn, W2PdSb, Zr2TiGe …
F. Heusler, Deutsche Physikalische Gesellschaft 5, p 219 (1903).
R. A. De Groot et al., Phys. Rev. Lett. 50, 2024 (1983).
Some of them are predicted HMM
E
E
EF
X
Y
Z

## Slide 3
Motivations
  High TC (> 700 K)
  Lattice constants
  HMM (ab initio calc.)
  I. Galanakis et al., Phys. Rev. B 66, 174429 (2002)
  Ultra low magnetic damping (ab initio calc.)
  B. Pradines et al., Phys. Rev. B 95, 094425 (2017)
  Experimentally confirmed in Co2MnSi
  M. Jourdan et al, Nature Comm. 5, 3974 (2014)
  S. Andrieu et al., Phys. Rev. B 93, 094417 (2016)
Co
Mn
Z
Why Co2Mn-based compounds ?

## Slide 4
Elaboration
Molecular Beam Epitaxy
Co2MnZ
MgO
Co-evap of each element (K-cells / e-guns)
Co2MnZ [100] (001) // MgO [110] (001)
450°C
Misfits < 5.4 %
Coalescence of 3D islands (Volmer-Weber)
800°C
Epitaxial relationship:
aMgO
aCo2MnZ
20 nm

## Slide 5
[110] RHEED patterns
Co2MnZ with Z=Al, Si, Ga, Ge, Sn, Sb
No half streaks = B2
Excellent surface quality
Al
Si
Ga
Ge
Sn
Sb

## Slide 6
STEM-HAADF
Si
Co2MnSi
Co
Mn
Si
L21
Co2MnSn
Co
Mn
Sn
L21 + (inverse)
Co2MnAl
Co
Mn / Al
B2

## Slide 7
Spin-Resolved PES
The Cassiopée Beamline
Mott detection SR-PES:
SOLEIL: 2,75 GeV storage ring, Saint Aubin, Fr.
MBE
(RHEED, AES)
SR-PES
AR-PES
2 e-guns (5 pockets)
4 effusion cells
Resolution 120 meV (for 30 eV)
Integration over 80 % of the BZ along

## Slide 8
Spin-Resolved PES
Co2MnZIV with ZIV=Si, Ge, Sn
Surface states S↑,↓
Polarization drops at EF
S↑,↓: symmetry
S. Andrieu et al., Phys. Rev. B 93, 094417 (2016)
Photon polarization: “p”
S. Andrieu et al., Phys. Rev. B 93, 094417 (2016)

## Slide 9
Symmetry & Spin-Resolved PES
Co2MnZIV with ZIV=Si, Ge, Sn
S↑,↓ no longer excited
Spin gaps
decreases with
Photon polarization: “s”
Consistent with ab initio calc.

## Slide 10
Spin-Resolved PES
Co2MnZIII with ZIII=Al, Ga
EF lowered in the band structure
S↑,↓ in empty states
Beginning of a spin gap
Consistent with ab initio calc.

## Slide 11
┴VNA-FMR
Co2MnGe
Vector Network Analyzer
Coplanar waveguide
sample
RF probe
Kittel:
Gilbert damping:
Effective values

## Slide 12
┴VNA-FMR
Ultra low damping values
T. Devolder et al., Appl. Phys. Lett. 103, 242410 (2013)
E
EF
E
EF
Anomaly
C. Guillemard et al., Phys. Rev. Appl. 11, 064009 (2019)

## Slide 13
Summary
Elaboration of 6 high quality epitaxial Heusler compounds
Spin gaps & ultra low magnetic damping values confirmed
Link between the Gilbert damping and the spin polarization

## Slide 14
S. Andrieu,
S, Mangin,
S. Petit-Watelot,
J.-L. Bello,
J.-C. Rojàs-Sanchez,
J. Ghanbaja,
L. Pasquier
F. Bertran,
P. Le Fèvre,
J. Rault
Thank you & collaborators
Organizers