## Slide 1: Micro-perforated membrane for label-free cell capture and integrated electrical detection operating in whole blood
Matthieu Sagota,b, Elise Boub, David Bourriera, Aline Cerfb,
Hervé Auberta, Christophe Vieua
a: LAAS-CNRS, Université de Toulouse, CNRS, INSA, INPT, 31400, Toulouse, France
b: SmartCatch, 1 Place Pierre Potier, 31100, Toulouse, France

## Slide 2
Dissemination of Circulating Tumor Biomarkers in Blood
Dying CTC
Phagocyte
Lymphocyte
Epithelial cell
Endothelial cell
Erythrocyte
Cancer cell after EMT
Cancer cell
Cancer stem-like cell
1
2
3
4
5
6
Blood Sample
Liquid Biopsy
Diagnosis, Prognosis
Treatment Response Monitoring
Anti-cancer substance assay
Primary tumor formation and growth
Epithelial to mesenchymal transition (EMT)
Intravasation
Spread of CTCs
Extravasation
Mesenchymal to epithelial transition (MET)
Secondary tumor formation and growth
Adapted from Melzer and al., 2017
1
2
3
4
5
6

## Slide 3
Combination of Cell Capture and Cell Detection
(Hz - kHz)
Capacitive behaviour: electrically insulating membrane
(500 kHz - 20 MHz)
Capacitive (membrane) and Conductive (cytoplasm) effects
(RF)
Access to the Conductive intracellular medium (cytoplasm)
Martisen, G. et Grimnes, S., Bioimpedance and bioelectricity basics, 2008
Electrical Properties of Biological Cells
Filtering Membrane
Blood Sample
Sensing Electrodes
CTC
17-52 µm
WBC
7 - 25 µm
RBC
6 µm

## Slide 4
E. Bou « Micro-dispositifs pour la biopsie liquide : vers la capture et détection intégrées de biomarqueurs cellulaires tumoraux ».
Microdevices Fabrication Process
Si
SiO2/Si3N4 0.8/0.6 µm
Au
0.8 µm
DF
5 µm
Ni
150 µm
1. Substrate Cleaning
2. CVD Deposition SiO2/Si3N4
Filtering Membrane
3. RIE Etching SiO2/Si3N4
4. RIE Etching SiO2/Si3N4
Openings for Connection Pads
5. Thermal Evaporation Au
Electrodes, Tracks and Connection Pads
6. RIE Etching SiO2/Si3N4
Pores Filtering Membrane
7. Electrolytic Deposition Au
Connection Pads Thickening
8. Dry Film Deposition DF
Tracks and Connection Pads Insulation
9. Electrolytic Deposition Ni
Supporting Structure
10. Substrate Wet Etching (KOH)
Device release
150 µm
1 mm
Connection Pads
Supporting Structure
Fluidic Slots
Filtering Membrane
Sensing Electrodes

## Slide 5: Cell Capture Experiments
Pre-Processing: Ethanol & PBS
Sample Processing: 10 min in closed loop
Post-Processing: Fixation and Observation
Blood (EFS – French Blood Collection Site)
Experimental Setup
Protocol

## Slide 6: Impedance Evolution during Sample Processing
0 min
10 min
Overlay Hoechst (Blue) and BF (Grey)
Impedance from 1kHz to 5MHz
Interface Impedance
Medium Impedance
•Impedance increases during sample
processing (200 kHz - 5 MHz)
•Good fit with a simple electrical model
•Stability of the Interface Impedance
•Evolution of the Medium Impedance in Blood
R2 > 0.99

## Slide 7: Detection of Captured Cells
Impedance Shift for various Media
Proteins
No Proteins / No Cells
Proteins + Cells
Capture and Detection Kinetics
•Detection of captured cells on the filtering membrane

## Slide 8: Conclusion and Prospects
We can selectively capture and detect in-situ cells in a whole blood sample without any pre-treatment !
Patent filed for integration into SmartCatch products intended for biology and pharmacology research fields
Detection of single cell capture events
Discrimination of CTCs based on their electrical signature

## Slide 9: Impedance Model for Electrical Measurements
Electrode-Electrolyte Interface
Probed Medium
Cole, K. S. Permeability and Imperbeability of Cell Membranes for Ions. Cold Spring Harb. Symp. Quant. Biol. 1940, 8 (0), 110–122.