Supplementary Material

Stability of monodomain III-V crystals and antiphase boundaries over a Si monoatomic step.

Divishth GUPTA a, Sreejith PALLIKKARA CHANDRASEKHARAN a, Simon THEBAUD a, Charles CORNET a,*, Laurent PEDESSEAU a,*

a Univ Rennes, INSA Rennes, CNRS, Institut FOTON – UMR 6082, F-35000 Rennes, France

* Corresponding author: charles.cornet@insa-rennes.fr (C. Cornet), laurent.pedesseau@insa-rennes.fr (L. Pedesseau)

Calculations details

In this work, all the calculations were performed using DFT implemented SIESTA code with a basis set of finite range of numerical atomic orbitals. We used the GGA-PBE gradient correction for the exchange correlation and norm-conserving pseudopotentials to represent the electron-ion interactions. The total energies of the unit cells and the heterostructures were calculated at an energy shift of 100meV with a 6x6x6 mesh and 150Ry cut off energy.

Bulk GaP and Si materials energies

Table S1: Stability of bulk Si and GaP with and without biaxial deformation. The total energy is calculated at an energy shift of 100meV with 6x6x6 mesh and 150Ry cut off energy.

|  | Si (Bulk) | GaP (Bulk) | GaP with biaxial deformation |
| --- | --- | --- | --- |
| Lattice constant (Å) | 5.48 | 5.62 | a=b=5.48 c=5.74 |
| No of atoms | 8 | 8 | 16 |
| Total energy (ev) | -1030.5614 | -8004.5237 | -16008.8011 |
| E/entity (eV) | -128.8201 | -2001.1309 | -2001.1001 |

Frozen and relaxed atoms in GaP/Si heterostructures

Figure S1: 2D representation of GaP/Si(001) heterostructure with a monatomic step at III/V interface depicting relaxed and constrained atoms. From left to right: Global structure, constrained atoms to mimic the bulk and relaxed atoms for a) abrupt interface with APBs (b) compensated interface with only Si-Ga interfacial layer, with APBs (c) abrupt interface without APBs and (d) compensated interface with Si-Ga and Si-P interfacial layer, without APB.