Supporting Information

Dimesitylboron as Electron Accepting Unit in High Performance Single-Layer Phosphorescent Organic Light Emitting Layer

Clément Brouillac, Fabien Lucas, Denis Ari, Christophe Lebreton, Olivier Jeannin, Joëlle Rault-Berthelot, Cassandre Quinton, Emmanuel Jacques, and Cyril Poriel*

C. Brouillac, D. Ari, J. Rault Berthelot, O. Jeannin, C. Quinton, C. Poriel

Univ Rennes, CNRS, ISCR-UMR CNRS 6226, F-35000 Rennes, France.
E-mail: cyril.poriel@univ-rennes.fr

F. Lucas
LPICM, CNRS, Ecole Polytechnique, IPParis, 91128 Palaiseau, France.

C. Lebreton, E. Jacques
Univ Rennes, CNRS, IETR-UMR CNRS 6164, F-35000 Rennes, France.

The materials and methods section with experimental details can be found in other works. [1, 2]  Synthesis

SPA-2-FBr was synthesized according to literature procedure.[3]

Synthesis of SPA-2-FDMB

SPA-2-FBr (2.00 g, 4.11 mmol, 1.0 eq) was dissolved in THF (150 mL) under argon atmosphere. Then, the mixture was cooled down to -78°C and n-butyllithium (2.50 M in hexanes, 4.28 mL, 10.7 mmol, 2.6 eq) was added dropwise at -78°C. The reaction was stirred for 1 h at -78 °C and dimesitylboron fluoride (2.87 g, 10.7 mmol, 2.6 eq) was added at once under strong flux of argon. The ice bath was directly removed and the reaction was under stirring at room temperature overnight. After, the reaction mixture was finally quenched with ethanoland the solvents were removed under reduced pressure. The crude was dissolved in DCM, washed 3 times with water, dried over Na2SO4 and filtered. Solvent was then evaporated under reduced pressure and the crude product was purified with flash chromatography on silica gel. After purification with flash chromatography on silica gel [column conditions: silica cartridge (80 g); solid deposit on Celite®; λdetection: (254 nm, 280 nm); gradient petroleum ether/CH2Cl2 from 100/0 to 80/20 in 60 min at 60 mL/min], the mixture was then purified by recycling size exclusion chromatography (CHCl3) giving the title compound as a yellowish powder (1.48 g, 55 %). 1H NMR (300 MHz, CDCl3) δ 7.89 – 7.84 (m, 1H), 7.79 – 7.69 (m, 2H), 7.64 – 7.33 (m, 7H), 7.10 – 7.03 (m, 2H), 6.93 (ddd, J = 8.5, 7.1, 1.6 Hz, 2H), 6.74 (s, 4H), 6.57 (ddd, J = 8.3, 7.1, 1.2 Hz, 2H), 6.46 (dd, J = 7.8, 1.6 Hz, 2H), 6.29 (dd, J = 8.3, 1.2 Hz, 2H), 2.28 (s, 6H), 1.85 (s, 12H). 13C NMR (75 MHz, CD2Cl2) δ 155.85, 155.53, 142.08, 141.65, 140.84, 140.68, 139.92, 138.49, 136.68, 134.19, 130.98, 130.95, 129.17, 128.22, 128.10, 127.97, 127.19, 126.52, 126.00, 125.08, 120.78, 120.33, 119.54, 114.62, 57.03, 23.16, 20.97. MALDI (m/z) calculated for C49H42NB [M]+: 655.340 found: 655.340.

[CCDC 2359045 contains the supplementary crystallographic data for this paper. These data can be obtained free of charge from The Cambridge Crystallographic Data Centre via www.ccdc.cam.ac.uk/data_request/cif.]

- Model Compound

Figure S 1 Model compound SPA-2-FPOPh2.

The synthetic procedure, the characterizations and its properties can be found in the literature.[3]

- Photophysical properties

Figure S 2 Absorption and emission spectra of SPA-2-FDMB in cyclohexane (left) and linear fit of the integration of the fluorescence between 395 and 525 nm as a function of the absorbance at 310 nm (right).

Figure S 3 Absorption and emission spectra of quinine sulfate in 1.0 N sulfuric acid (left) and linear fit of the integration of the fluorescence between 380 and 580 nm as a function of the absorbance at 310 nm (right).

|  | Quinine sulfate in 0.1 N sulfuric acid | SPA-2-FDMB in cyclohexane |
| --- | --- | --- |
| Slope | 5.76 × 108 | 8.45 × 106 |
| Refractive index | 1.336 | 1.427 |
| QY | 0.546 | 0.01 |

Figure S 4  Fluorescence decay in cyclohexane (λexc=310 nm, λem=500 nm, left) at RT and phosphorescence decay in a frozen matrix of 2-MeTHF at 77 K (λexc=350 nm, λem=500 nm, right) of SPA-2-FDMB.

Figure S 5 Absorption spectra of SPA-2-FDMB in various solvents.

Figure S 6 Absorption and emisison spectra of SPA-2-FPOPh2 in various solvents.

Figure S 7 Absorption (left) and emission (right, λexc=350 nm) of SPA-2-DFDMB in spin-coated thin film.

Figure S 8 Absorption (left) and emission (right, λexc=400 nm) of a mixture of SPA-2-FDMB (w=90%) and PO-01 (w=10%) in spin-coated thin film.

Figure S 9 TOP. Absorption  (dichloromethane, RT, black line), fluorescence (dichloromethane, RT, red line, λexc=440 nm) and phosphorescence (2-MeTHF, 77 K, green line, λexc=440 nm) of PO-01. Bottom. TGA of PO-01 (Td= 372°C)

RT => ET=2.22 eV / λ=558 nm

77K => ET=2.28 eV  /  λ=545 nm (E(eV)=1239.84 / λ (m) )

Table S 1 Lippert-Mataga formalism calculation of SPA-2-FDMB in various solvents.

| Solvent | labs (nm) | lem (nm) | nabs (cm-1) | nem (cm-1) | Dn (cm-1) | e | n | Df |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cyclohexane | 347 | 433 | 28818.4438 | 23094.68822 | 5723.76 | 2.02 | 1.426 | -0.0016 |
| Chloroforme | 348 | 484 | 28735.63218 | 20661.15702 | 8074.48 | 4.81 | 1.446 | 0.1482 |
| DCM | 347 | 508 | 28818.4438 | 19685.03937 | 9133.40 | 8.93 | 1.424 | 0.2172 |
| THF | 348 | 503 | 28735.63218 | 19880.71571 | 8854.92 | 7.58 | 1.4072 | 0.2096 |
| ACN | 345 | 544 | 28985.50725 | 18382.35294 | 10603.15 | 37.5 | 1.344 | 0.3055 |

Table S 2 Lippert-Mataga formalism calculation of SPA-2-FPOPh2 in various solvents

| Solvent | labs (nm) | lem (nm) | nabs (cm-1) | nem (cm-1) | Dn (cm-1) | e | n | Df |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cyclohexane | 315 | 402 | 31746.03175 | 24875.62189 | 6870.41 | 2.02 | 1.426 | -0.0016 |
| Chloroforme | 325 | 484 | 30769.23077 | 20661.15702 | 10108.07 | 4.81 | 1.446 | 0.1482 |
| DCM | 320 | 457 | 31250 | 21881.83807 | 9368.16 | 8.93 | 1.424 | 0.2172 |
| THF | 318 | 442 | 31446.54088 | 22624.43439 | 8822.11 | 7.58 | 1.4072 | 0.2096 |
| ACN | 321 | 518 | 31152.64798 | 19305.01931 | 11847.63 | 37.5 | 1.344 | 0.3055 |

Figure S 10 Lippert-Mataga formalism linear fit for SPA-2-FDMB (black) and SPA-2-FPOPh2 (red).

Table S 3 Summary of the radius of the solvation sphere (r), dipole moment at the ground (μ) and excited (μ*) states and the difference (Δμ) for SPA-2-FDMB and SPA-2-FPOPh2.

|  | r(Å) | Δµ (D) | µ (D) | µ* (D) |
| --- | --- | --- | --- | --- |
| SPA-2-FDMB | 6.5 | 20.5 | 1.4 | 21.4 |
| SPA-2-FPOPh2 | 5.7 | 16.0 | 5.4 | 21.9 |

- Electrochemical properties

Figure S 11 Cyclic voltammetries recorded on Pt working electrode in reduction  (left, DMF + Bu4NPF6 0.1 m, sweep-rate 100 mV s-1) and in oxidation (right, CH2Cl2 + Bu4NPF6 0.2 m, sweep-rate 100 mV s-1) of SPA-2-FDMB.

Figure S 12  Cyclic voltammogram (left) and differential pulse voltammogram (right) recorded in CH2Cl2 + Bu4NPF6 0.2 M in presence of PO-01

Figure S 13 Cyclic voltammogram (left) and differential pulse voltammogram (right) recorded in CH2Cl2 + Bu4NPF6 0.2 M in presence of PO-01 5exclusively the first oxidation wave).

Figure S 14 Cyclic voltammogram (left) and differential pulse voltammogram (right) recorded in DMF + Bu4NPF6 0.1 M in presence of PO-01 (exclusively the first reduction wave)

HOMO (PO-01) = -5.03 eV (determined by oxidation in DCM)

LUMO (PO-01) = -2.41 eV (determined by reduction in DMF)

- Molecular modeling

Table S 4 Atomic coordinates of SPA-2-FDMB at the fundamental state after geometry optimization (b3lyp/6-31g(d))

| Atoms | X (Å) | Y (Å) | Z (Å) |
| --- | --- | --- | --- |
| C | -0.673069 | 1.827987 | -0.240358 |
| C | -0.29281 | 3.15741 | -0.505161 |
| C | -1.500135 | 3.99044 | -0.548925 |
| C | -2.620892 | 3.171507 | -0.311009 |
| C | -2.204466 | 1.712309 | -0.0886 |
| C | 0.27943 | 0.82561 | -0.163409 |
| C | 1.653239 | 1.12128 | -0.324933 |
| C | 2.008042 | 2.468153 | -0.575198 |
| C | 1.056289 | 3.480782 | -0.679128 |
| C | -2.773329 | 0.776792 | -1.161652 |
| C | -3.09006 | -0.563618 | -0.859647 |
| N | -3.003919 | -1.035664 | 0.464717 |
| C | -2.887039 | -0.138043 | 1.544769 |
| C | -2.564235 | 1.215305 | 1.316288 |
| C | -1.658396 | 5.360507 | -0.776912 |
| C | -2.945183 | 5.90106 | -0.764142 |
| C | -4.058263 | 5.085173 | -0.527614 |
| C | -3.90082 | 3.713955 | -0.299777 |
| C | -3.214238 | -2.432702 | 0.730493 |
| C | -4.507224 | -2.929676 | 0.930807 |
| C | -4.700253 | -4.286753 | 1.192642 |
| C | -3.603954 | -5.150003 | 1.256529 |
| C | -2.314459 | -4.653279 | 1.056333 |
| C | -2.116841 | -3.296541 | 0.791617 |
| C | -2.890138 | 1.213307 | -2.486862 |
| C | -3.296789 | 0.363248 | -3.511264 |
| C | -3.593907 | -0.965397 | -3.206736 |
| C | -3.495379 | -1.424504 | -1.898581 |
| C | -3.093755 | -0.581249 | 2.865896 |
| C | -2.993788 | 0.29943 | 3.936593 |
| C | -2.691208 | 1.64331 | 3.717186 |
| C | -2.47928 | 2.080832 | 2.4132 |
| C | 1.272563 | -3.173748 | -2.010197 |
| C | 1.444895 | -4.185242 | -1.063312 |
| C | 2.048073 | -3.841202 | 0.148431 |
| C | 2.478936 | -2.537482 | 0.420835 |
| C | 2.286437 | -1.505431 | -0.536531 |
| C | 1.662216 | -1.852676 | -1.765851 |
| B | 2.734403 | -0.010063 | -0.243711 |
| C | 4.228769 | 0.372934 | 0.124636 |
| C | 4.5285 | 1.070601 | 1.325502 |
| C | 5.853276 | 1.3946 | 1.640325 |
| C | 6.914756 | 1.083787 | 0.78984 |
| C | 6.61803 | 0.404846 | -0.394355 |
| C | 5.31243 | 0.037005 | -0.732362 |
| C | 5.10377 | -0.693877 | -2.043776 |
| C | 8.332419 | 1.481014 | 1.12732 |
| C | 1.403099 | -0.84438 | -2.871485 |
| C | 0.983687 | -5.597177 | -1.339985 |
| C | 3.116914 | -2.274394 | 1.770255 |
| C | 3.4615 | 1.473479 | 2.32829 |
| H | -0.02356 | -0.200731 | 0.025324 |
| H | 3.059157 | 2.715651 | -0.699436 |
| H | 1.361844 | 4.503272 | -0.888084 |
| H | -0.796702 | 5.996905 | -0.96132 |
| H | -3.084604 | 6.96447 | -0.939499 |
| H | -5.053643 | 5.521208 | -0.5209 |
| H | -4.765671 | 3.08209 | -0.116297 |
| H | -5.350949 | -2.247457 | 0.880646 |
| H | -5.705741 | -4.668441 | 1.347667 |
| H | -3.754919 | -6.206202 | 1.46252 |
| H | -1.45748 | -5.319033 | 1.108242 |
| H | -1.116779 | -2.904958 | 0.631072 |
| H | -2.644208 | 2.245639 | -2.716009 |
| H | -3.373416 | 0.732088 | -4.529861 |
| H | -3.910176 | -1.652425 | -3.987298 |
| H | -3.735951 | -2.456589 | -1.675597 |
| H | -3.33733 | -1.620158 | 3.050632 |
| H | -3.159555 | -0.071006 | 4.944856 |
| H | -2.613155 | 2.339543 | 4.547021 |
| H | -2.228834 | 3.121854 | 2.233832 |
| H | 0.819951 | -3.417518 | -2.970275 |
| H | 2.202782 | -4.612785 | 0.900927 |
| H | 6.059511 | 1.904838 | 2.580018 |
| H | 7.429052 | 0.14442 | -1.072535 |
| H | 6.061852 | -0.878719 | -2.54015 |
| H | 4.606053 | -1.657545 | -1.899907 |
| H | 4.484627 | -0.115052 | -2.740436 |
| H | 8.472818 | 1.58757 | 2.208277 |
| H | 8.596039 | 2.443819 | 0.668607 |
| H | 9.054324 | 0.742132 | 0.762033 |
| H | 0.408781 | -0.39199 | -2.773424 |
| H | 1.443156 | -1.333478 | -3.851058 |
| H | 2.124152 | -0.02336 | -2.87906 |
| H | 1.443018 | -6.311754 | -0.648735 |
| H | -0.105904 | -5.688013 | -1.234445 |
| H | 1.232299 | -5.907775 | -2.361323 |
| H | 4.105935 | -1.817389 | 1.672385 |
| H | 2.50928 | -1.596483 | 2.382941 |
| H | 3.228433 | -3.206017 | 2.334342 |
| H | 3.896514 | 1.578634 | 3.328074 |
| H | 3.005407 | 2.435277 | 2.065509 |
| H | 2.644843 | 0.749704 | 2.396097 |

Number of negative frequencies : 0

Table S 5 Results of TD-DFT calculations for SPA-2-FDMB (b3lyp/6-311+g(d,p)).

| Wavelength (nm) | Osc, Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- |
| 452 | 0.0004 | HOMO->LUMO (99%) |  |
| 359 | 0.2222 | H-2->LUMO (55%), H-1->LUMO (40%) |  |
| 357 | 0.1885 | H-2->LUMO (42%), H-1->LUMO (45%) | H-4->LUMO (5%), H-3->LUMO (5%) |
| 341 | 0.0003 | HOMO->L+2 (62%), HOMO->L+3 (36%) |  |
| 339 | 0.0319 | H-3->LUMO (89%) | H-4->LUMO (4%), H-1->LUMO (4%) |
| 332 | 0.0095 | HOMO->L+1 (14%), HOMO->L+2 (34%), HOMO->L+3 (51%) |  |
| 330 | 0.0047 | H-5->LUMO (29%), H-4->LUMO (60%) | H-6->LUMO (2%), H-1->LUMO (4%) |
| 329 | 0.0058 | H-5->LUMO (68%), H-4->LUMO (25%) |  |
| 326 | 0.018 | HOMO->L+1 (70%), HOMO->L+4 (18%) | HOMO->L+3 (9%) |
| 312 | 0.0026 | HOMO->L+1 (14%), HOMO->L+4 (76%) | HOMO->L+3 (3%), HOMO->L+5 (2%) |
| 310 | 0.0564 | H-6->LUMO (21%), HOMO->L+5 (65%) | H-1->L+1 (4%) |
| 306 | 0.1227 | H-6->LUMO (57%), HOMO->L+5 (26%) | H-1->LUMO (2%), H-1->L+1 (5%) |
| 299 | 0.0571 | HOMO->L+6 (88%) | H-7->LUMO (8%) |
| 297 | 0.0099 | H-7->LUMO (89%) | HOMO->L+6 (8%) |
| 287 | 0.0255 | H-9->LUMO (21%), H-8->LUMO (64%) | H-6->LUMO (4%), H-1->L+6 (4%) |
| 280 | 0.0059 | H-9->LUMO (65%), H-8->LUMO (26%) | H-1->L+1 (3%) |
| 276 | 0.0748 | H-1->L+1 (49%), H-1->L+4 (11%) | H-12->LUMO (3%), H-11->LUMO (9%), H-9->LUMO (5%), H-6->LUMO (9%) |
| 273 | 0.0793 | HOMO->L+9 (12%), HOMO->L+10 (58%), HOMO->L+11 (10%) | H-7->L+6 (2%), HOMO->L+7 (6%), HOMO->L+12 (2%) |
| 271 | 0.0049 | HOMO->L+7 (77%), HOMO->L+9 (19%) |  |
| 269 | 0.0128 | HOMO->L+8 (77%) | HOMO->L+9 (8%), HOMO->L+10 (4%), HOMO->L+11 (6%) |

- PhOLED devices

Figure S 15  Energy diagram of the various EML constituents in the yellow SL-PhOLEDs (left). CIE diagram with PO-01 coordinates (right).

Figure S 16   Comparison between photoluminescence and electroluminescence spectra (mixture of SPA-2-FDMB (w=90%) and PO-01 (w=10%))

- X-Ray parameters

Table S 6 Crystal data and structure refinement for SPA-2-FDMB.

| Empirical formula | C49 H42 N2 |  |
| --- | --- | --- |
| Formula weight | 658.84 |  |
| Temperature | 150(2) K |  |
| Wavelength | 0.71073 Å |  |
| Crystal system | Triclinic |  |
| Space group | P -1 |  |
| Unit cell dimensions | a = 11.0306(9) Å | a= 76.767(3)°. |
|  | b = 13.4858(12) Å | b= 71.413(3)°. |
|  | c = 13.8875(14) Å | g = 71.040(3)°. |
| Volume | 1833.7(3) Å3 |  |
| Z | 2 |  |
| Density (calculated) | 1.193 Mg/m3 |  |
| Absorption coefficient | 0.069 mm-1 |  |
| F(000) | 700 |  |
| Crystal size | 0.31 x 0.29 x 0.24 mm3 |  |
| Theta range for data collection | 2.205 to 27.492°. |  |
| Index ranges | -14<=h<=14, -17<=k<=17, -18<=l<=18 |  |
| Reflections collected | 44596 |  |
| Independent reflections | 8380 [R(int) = 0.0444] |  |
| Completeness to theta = 25.242° | 99.70% |  |
| Refinement method | Full-matrix least-squares on F2 |  |
| Data / restraints / parameters | 8380 / 0 / 467 |  |
| Goodness-of-fit on F2 | 0.726 |  |
| Final R indices [I>2sigma(I)] | R1 = 0.0684, wR2 = 0.2004 |  |
| R indices (all data) | R1 = 0.0767, wR2 = 0.2182 |  |
| Extinction coefficient | 0.022(4) |  |
| Largest diff. peak and hole | 0.448 and -1.218 e.Å-3 |  |

- Copy of NMR spectra

All the NMR spectra 1H, 13C and 13C DEPT-135 of SPA-2-FBr can be found in literature. [3]

Figure S 17 1H NMR (top) and 13C NMR (bottom) spectra of SPA-2-FDMB.

- Copy of mass spectra

Figure S 18 HRMS (MALDI) spectra of SPA-2-FDMB.

- References

[1] F. Lucas, D. Tondelier, B. Geffroy, T. Heiser, O. A. Ibraikulov, C. Quinton, C. Brouillac, N. Leclerc, J. Rault-Berthelot, C. Poriel, Mater. Chem. Front. 2021, 5, 8066.

[2] C. Brouillac, F. Lucas, D. Ari, D. Tondelier, J. Meot, M. Malvaux, C. Jadaud, C. Lebreton, J. Rault-Berthelot, C. Quinton, E. Jacques, C. Poriel, Adv. Electron. Mater 2024, 10, 2300582.

[3] F. Lucas, C. Quinton, S. Fall, T. Heiser, D. Tondelier, B. Geffroy, N. Leclerc, J. Rault-Berthelot, C. Poriel, J. Mater. Chem. C 2020, 8, 16354.